Tendencias en biopolímeros como materiales de envase de productos farmacéuticos. Una revisión

Trends in biopolymers as packaging materials for pharmaceutical products. A review

Nelson Daniel Pinzón-Neira

Rodrigo Rey-Galindo

RESUMEN

Los biopolímeros provienen de elementos renovables de la naturaleza; es decir, son de origen bio base y se degradan por microorganismos naturales como bacterias, hongos y algas en condiciones ambientales. En la actualidad, estos biopolímeros se utilizan en el desarrollo de múltiples tecnologías en diferentes campos de investigación, por ejemplo: biomedicina, industria farmacéutica, empaque de alimentos y productos en general, entre otros. El objetivo de esta revisión consiste en identificar los diferentes biopolímeros que han sido resultado de investigaciones entre los años 2008 y 2022, establecer los países con mayor número de publicaciones, los materiales más investigados y las aplicaciones dadas a cada material. Finalmente se clasifican los biopolímeros según su forma de obtención y sus aplicaciones como envase en la industria farmacéutica. Para el desarrollo de esta investigación, se utilizó la metodología de análisis de contenido, apoyada en la hermenéutica general y el paradigma interpretativo. En los resultados se puede observar qué las publicaciones sobre biopolímeros están ascendiendo año a año, los materiales que más se implementan para su desarrollo son: Celulosa, Quitosan y Ácido Poliláctico, y sus aplicaciones más comunes son para empaque de alimentos, biomedicina y empaque en general. Se concluye que los avances científicos en la línea de lo biopolímeros son un buen escenario para disminuir el consumo de plásticos convencionales y con menor impacto ambiental, además de las garantías en campos como los empaques de alimentos, la biomedicina y para envases de productos farmacéuticos, dado que no son tóxicos y son biodegradables.

PALABRAS CLAVE: Bioplástico, Biodegradación, Biopolímero, Material de empaque, Nanocompuestos, PLA.

ABSTRACT

Biopolymers come from renewable elements in nature; that is, they are of bio-based origin and are degraded by natural microorganisms such as bacteria, fungi and algae under environmental conditions. Currently, these biopolymers are used in the development of multiple technologies in different fields of research, for example: biomedicine, pharmaceutical industry, food packaging and products in general, among others. The objective of this review is to identify the different biopolymers that have been the result of research between 2008 and 2022, establish the countries with the greatest number of publications, the most researched materials and the applications given to each material. Finally, biopolymers are classified according to how they are obtained and their applications as packaging in the pharmaceutical industry. To develop this research, the content analysis methodology was used, supported by general hermeneutics and the interpretive paradigm. In the results it can be seen that publications on biopolymers are increasing year by year, the materials that are most implemented for their development are: Cellulose, Chitosan and Polylactic Acid, and their most common applications are for food packaging, biomedicine and packaging in general. It is concluded that scientific advances in the line of biopolymers are a good scenario to reduce the consumption of conventional plastics with less environmental impact, in addition to guarantees in fields such as food packaging, biomedicine and for pharmaceutical product packaging, since they are non-toxic and biodegradable.

KEY WORDS: Bioplastic, Biodegradation, Biopolymer, Packaging material, Nanocomposites, PLA.

- Introducción

La producción de envases representa la mayor aplicación de plásticos en la actualidad (Lagaron y Lopez-Rubio, 2010). Para el 2015 esta producción derivada del petróleo superó los 300 millones de toneladas (Mellinas et al. 2015). Cada año se generan 34 millones de toneladas de plásticos como residuos sólidos (Mekonnen et al. 2013). Geyer y otros (2017) estiman que desde 1950 hasta 2015 se produjeron 6.300 Millones de toneladas de residuos plásticos acumulados, de los cuales 9% han sido reciclados, 12% se incineraron, y 79% han terminado en los océanos y vertederos o sitios destinados de disposición final. Es así que, de cada kilogramo de plástico quemado puede generar hasta 2,8 Kg de CO2 (Mellinas et al. 2015) lo que agudiza la problemática del cambio climático.

La producción de envases representa la mayor aplicación de plásticos en la actualidad (Lagaron y Lopez-Rubio, 2010) y una carga importante como contaminación ambiental por su participación en los residuos sólidos municipales (UNEP, 2024). Para el 2015 esta producción derivada del petróleo superó los 300 millones de toneladas (Mellinas et al. 2015).

Es importante señalar que los productos manufacturados de materiales renovables para envases ocupan solo el 2% del mercado mundial (Johansson et al. 2012), esto se debe, a que los biopolímeros presentan bajas propiedades de resistencia mecánicas, térmicas y de barrera para medicamentos en comparación a los materiales petroquímicos convencionales.

Además, es necesario tener en cuenta que los combustibles convencionales de petróleo han disminuido su disponibilidad, lo que aumenta su costo con pronóstico de posible escasez (Davis y Song, 2006; Hernández-Silva y Guzmán Martínez, 2009). Para satisfacer la creciente demanda de sostenibilidad y seguridad ambiental, un número significativo de investigaciones se han dirigido al desarrollo de materiales de envasado y empaque, que pueden degradarse rápidamente y mineralizarse por completo en el medio ambiente y disminuir su impacto ambiental negativo (Jayaramudu et al. 2013; Ortega-Santiago et al. 2023). El resultado de estas investigaciones son los bioplásticos provenientes de elementos renovables en la naturaleza como la celulosa, el almidón y el azúcar (Meeks et al. 2015), estos plásticos se degradan por microorganismos naturales como bacterias, hongos y algas; acompañado de condiciones ambientales como temperatura, agua y oxígeno (Thakur et al. 2018). Al realizar la presente investigación sobre los bioplásticos, como materiales de envase para medicamentos, se evidencia el comportamiento productivo de estos, así como los avances y desarrollo sobre el tema.

De otra parte, los envases para medicamentos se diferencian de dos maneras. Existe el denominado “envase primario” que es el contenedor que está en contacto directo con el medicamento, fabricado con materiales de naturaleza variada, diseñado de modo que brinde información y óptima protección a su contenido, así como al medio ambiente (Orantes y Hernández, 2006) Y los llamados “envases de segundo tipo”, son aquellos que se utilizan como embalaje de productos para evitar averías en el envase primario, cuidados especiales del producto o como medida preventiva, y para brindar mayor información al cliente o usuario sobre el medicamento (Borja y Eva, 2006).

En cuanto a los bioplásticos, estos pueden ser un biopolímero derivado de la naturaleza o un polímero que puede retornar a la naturaleza. Su fabricación se asocia a materiales 100% renovables, polímeros biodegradables o una combinación de materiales renovables y fósiles (Reddy, M, et al. (2013). Los biopolímeros son polímeros formados por la naturaleza durante los ciclos de crecimiento de los organismos, se les conoce como polímeros naturales, su síntesis generalmente implica reacciones de polimerización de crecimiento en cadena catalizados por enzimas de monómeros activos, que se forman dentro de las células mediante procesos metabólicos complejos (Zhang Y. et al. 2013).

En este sentido, los polímeros biodegradables se pueden dividir según su origen en cuatro categorías: (1) polímeros directamente de la biomasa, incluidos los polisacáridos como, quitosano, almidón, celulosa y las proteínas como, zeína; (2) polímeros sintéticos basados en monómeros petroquímicos, tales como poli E-caprolactona, poli adipato-co-tereftalato de butileno y poli alcohol vinílico (PVOH); (3) polímeros sintéticos basados en monómeros renovables, por ejemplo polilactida (PLA); (4) polímeros naturales producidos por microorganismos, típicamente polihidroxialcanoatos (PHA) tales como poli 3-hidroxibutirato (PHB) y poli (PHBV) (Lagarón y Busolo, 2011; Martínez et al. 2019).

La mayor parte de las investigaciones que se han realizado sobre biopolímeros en relación con su base biológica y biodegradable se refieren al almidón, PLA, poli (3-hidroxibutirato) (PHB) y sus mezclas. Si bien la rigidez y la resistencia de estos suelen ser grandes, su aplicación a menudo está limitada por el proceso, la sensibilidad al agua y la baja resistencia al impacto (Imre y Pukánszky, 2013).

El poli (ácido láctico) recibió mucha atención en los últimos años como una de las alternativas más prometedoras a los plásticos convencionales (Auras et al. 2004). Sus propiedades mecánicas son comparables a las del poli-estireno, y como consecuencia, se utiliza en cantidades cada vez mayores en aplicaciones de envasado (Martin y Avérous, 2001). El representante más común de los PHA, es el poli (3-hidroxibutirato), es un polímero quebradizo, dado que su polimerización enzimática conduce a la formación de macromoléculas con una estructura estereoquímica altamente ordenada, por lo tanto, gran cristalinidad (Sudesh et al. 2000). Aunque el aumento de las capacidades da como resultado una producción confiable y un precio decreciente de los biopolímeros, su costo aún supera el de la mayoría de los polímeros comerciales (Imre y Pukánszky, 2013).

El objetivo de esta investigación es identificar las tendencias mundiales de bioplásticos aplicados a envases de medicamentos en el periodo 2008 a 2022. Se van a reconocer los bioplásticos según el recurso de origen y el producto que se obtenga de este. Luego se clasifican por las aplicaciones industriales que se realizan a cada material en particular para envases farmacéuticos. Finalmente se identifica el biopolímero de mayor investigación para la práctica en uso como envase farmacéutico.

- Metodología

La presente revisión se encuentra fundamentada en la metodología de Análisis de Contenido (Bardín, 1996; Fernández, 2002; López-Noguero, 2002; Valbuena-Ussa, 2011; Hernández y Mendoza, 2018). Además, se apoya en la hermenéutica general (Grondin, 2014) y el paradigma interpretativo (Vasilachis de Gialdino, 2006). Con el fin de construir la interpretación conceptual que permite inferir la dirección de las investigaciones consultadas y analizadas sobre biopolímeros en el mundo.

Se aplicó, a 196 artículos de investigación sobre empaques biopolímeros en una escala temporal entre los años 2008 a 2022 (15 años). Las bases de datos para identificar los documentos fueron Scopus, Science Direct y Springer Link.

Sobre los documentos identificados se realizó una sistematización que permitió establecer las categorías explicativas. El filtro inicial se tomó como frase clave “Biopolymer packaging pharmaceutical”, al obtener 14.032 artículos (Scopus 1%, Springer Link 36%, Science Direct 63%), al especificar el periodo de tiempo se identificaron 8.269 artículos como universo.

La búsqueda inicial se realizó por temáticas por cada base de datos de la siguiente manera, para Scopus: “Chemistry” “Engineering”; para Springer Link: “Chemistry” “Polimeric science” “Engineering”; y para Science Direct: “Chemistry” “Engineering”. Luego, se concentró en los artículos con al menos una de las siguientes palabras claves en el título, como unidades de análisis: “biopolymer”, “packaging”, “drugs”, “composites”, “biomaterial”. Lo que permitió obtener 201 artículos. Se encontraron cinco artículos duplicados. Finalmente, el análisis de contenido y la inferencia interpretativa se concentró en la revisión de 196 documentos.

La información recolectada se clasificó según una adaptación del análisis Clúster Jerárquico (Kaufman y Rousseeuw, 2005) con grupos reconocidos, para encontrar clasificaciones por segmentos a partir de sus características. La pertinencia documental, se basó en hallar documentos con información del objeto de la revisión, inicialmente con una frase de búsqueda (biopolymer+packaging+pharmaceutical), con la temporalidad entre 2008-2022 (Tabla 1).

Tabla 1. Clúster inicial

| FASE INICIAL |  |  | AREA DE ESTUDIO |  |  | PALABRAS CLAVE |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BASES DE DATOS | BIOPOLIMER+PACKAGING+PHARMACEUTICAL | AÑO (2008-2022) | CHEMISTRY | ENGINEERING | POLIMERIC SCIENCE | 1 | 2 | 3 | SUB TOTAL |
| SCOPUS | 188 | 126 | 42 | 12 | 0 | 13 | 8 | 1 | 22 |
| SCIENCE DIRECT | 8825 | 4551 | 492 | 169 | 0 | 56 | 19 | 1 | 76 |
| SPRINGER LINK | 5019 | 3592 | 335 | 48 | 269 | 78 | 15 | 5 | 98 |
| SUBTOTAL | 14032 | 8269 | 869 | 229 | 269 | 147 | 42 | 7 | 196 |
| TOTAL | 14032 | 8269 | 1367 |  |  | 196 |  |  |  |

Como categorías de análisis, para cada uno de los artículos seleccionados, se formularon criterios relacionados con Autores, Año de publicación, País de origen, Biopolimero utilizado, Origen del biopolímero, Forma de obtención, y Aplicación del insumo. Para los artículos tipo revisión se filtró por la expresión “Biopolímeros”, para estos artículos se estableció y cuantificó, el origen, forma de obtención y aplicación del biopolímero.

La presente investigación profundizó en la información clave sobre los biopolímeros, la cual se encuentra en el contenido estructural de los artículos de investigación que se analizaron. Además, se incluyó el tipo de biopolímero, su origen, forma de obtención y aplicación. En varios de estos artículos se encontraron múltiples hallazgos sobre los materiales.

- Resultados

  - Tendencias en Investigación de Biopolímeros

Para analizar el comportamiento de las publicaciones sobre biopolímeros durante quince años (2008-2022) se utilizó el método estadístico de dispersión lineal. Se evidencia un comportamiento ascendente en publicaciones sobre la temática año a año (Figura 1). El año con mayor número de artículos es 2022 con 19% de los documentos registrados.

Fig. 1. Publicaciones al año sobre Biopolímeros

El comportamiento de la revisión por países, muestra que India es el país que más ha publicado en el periodo tiempo analizado con 33 artículos, seguido de China con 14 artículos y Brasil con 13 (Tabla 2). En la presente revisión se determinó que las empresas exportadoras de materiales para pruebas químicas de biopolímeros son de Estados Unidos, Canadá e India. Este último se ha especializado en el desarrollo académico de los biopolímeros con la cooperación de Universidades locales y colaboración internacional.

Tabla 1. Temáticas de publicación por país

| PAÍS | POLIMERO | REFERENCIAS |
| --- | --- | --- |
| ALEMANIA Total (5) | PULLULAN | Gutiérrez y Alvarez (2017). |
|  | PLA | Kale et al. (2007); Mallakpour y Jarang (2018). |
|  | BIOMASA | Friedrich (2022). |
|  | NANOPARTICULAS | Ghanbari Adivi et al. (2019). |
|  | PPC | Henke et al. (2017). |
| ARABIA SAUDI Total (4) | PHA | Rajan et al. (2018). |
|  | CMC | Ahmed et al. (2022). |
|  | NANOCOMPUESTOS | Wazzan (2021). |
|  | QUITOSAN | Abutalib y Rajeh (2021). |
| ARGENTINA Total (3) | QUITOSAN | Ansorena et al. (2018). |
|  | CELULOSA | Villarreal et al. (2021); de Oliveira et al. (2021). |
|  | QUITOSAN | Favatela et al. (2022). |
| BRASIL Total (13) | PHA-PLG | Fasciotti (2017). |
|  | BIOPOLIMEROS | de Mesquita et al. (2010); Alves Lopes et al. (2020); Parente et al. (2023); Núñez-Gómez et al. (2021); da Rosa et al. (2020). |
|  | PLA | Lopes et al. (2012). |
|  | PVA | Silva et al. (2008). |
|  | QUITOSAN | de Mesquita et al. (2010). |
|  | CELULOSA | Meneguin et al. (2020). |
|  | NANOCOMPUESTOS | Rodrigues et al. (2020); Kostag et al. (2019). |
| CANADA Total (6) | BIOPOLIMEROS | Shen et al. (2014); Soares et al. (2018). |
|  | GELATINA | Duquette y Dumont (2019). |
|  | PULLULAN | Miao y Hamad (2013). |
|  | PLA | Chow et al. (2008). |
|  | PBS-PBAT | Muthuraj et al. (2014). |
|  | QUITOSAN | Akhlaghi et al. (2013). |
| CHILE | CELULOSA | Oyarce et al. (2022). |
| CHINA Total (14) | CELULOSA | Wang Y. et al. (2018). |
|  | PLA | Zhang Q. et al. (2018); Xian et al. (2018); Xie et al. (2014); Wang X. et al. (2014). |
|  | PHMC | Hu et al. (2018). |
|  | BIOPOLIMEROS | Xing et al. (2021); Qiu et al. (2021); AL‑Oqla et al. (2022); He et al. (2020). |
|  | NANO PARTICULAS | Wang D-Y. et al. (2022); Hashim et al. (2022). |
|  | POLIFENOLES | Zhang D. et al. (2021). |
|  | QUITOSAN | Jiang et al. (2022); Zhao et al. (2022); Dong et al. (2022); Zou et al. (2020). |
| COLOMBIA Total (2) | NANOFIBRAS | Rodríguez-Sánchez et al. (2021). |
|  | PHA | Vega‑Castro et al. (2021). |
| COREA | BIOPOLIMEROS | Rhim et al. (2007). |
| DINAMARCA | CELULOSA | Siró y Plackett (2010). |
| EGIPTO Total (6) | PVA | El-Gamal et al. (2018). |
|  | QUITOSAN | Elhussieny et al. (2020); Ahmed M. K. et al. (2021). |
|  | CELULOSA | Elhussieny et al. (2020). |
|  | NANOPARTICULAS | Moustafa et al. (2022). |
|  | BIOPOLIMEROS | Ibrahim S. et al. (2021). |
| ESPAÑA Total (8) | ALGINATO | Serrano-Aroca et al. (2018). |
|  | BIOPOLIMEROS | L. Quiles-Carrillo et al. (2019); Aznar et al. (2019). |
|  | PLA | Perez-Masia et al. (2013) |
|  | NANO PARTICULAS | Abdullah et al. (2022). |
|  | POLISACÁRIDOS | Rincon et al. (2021). |
|  | OLIGOMEROS | Ubeda et al. (2021). |
| ESTADOS UNIDOS Total (6) | CELULOSA | Janjarasskul y Krochta (2010). |
|  | BIOPOLIMEROS | Williamson y Hatzakis (2019); Virtanen et al. (2017); Kumar A. P. et al. (2009); Bandyopadhyay-Ghosh et al. (2018); Farris et al. (2009); Correa et al. (2016); Biswas et al. (2022). |
|  | PLA | Correa et al. (2016); Resano-Goizueta et al. (2018); Satam et al. (2018). |
|  | PHA | York et al. (2008). |
|  | PHA-PLG | Zhang Y. et al. (2013). |
| FRANCIA Total (2) | PLA | Chauvet et al. (2017). |
|  | BIOPOLIMEROS | Paul et al. (2021). |
| GRECIA | PLA | Liarou et al. (2018). |
| HOLANDA Total (2) | BIOPOLIMEROS | Mooibroek et al. (2007). |
|  | GELATINA | Scholten et al. (2014). |
| HUNGRÍA Total (3) | PLA | Vidovic (2016). |
|  | BIOPOLIMEROS | Yi et al. (2022); Takács et al. (2020). |
| INDIA Total (33) | CELULOSA | Neera y Batra (2015); Mishra R. K. et al. (2018); Mishra D. et al. (2021); Kalyani y Khandelwal (2021). |
|  | BIOPOLIMEROS | Luckachan y Pillai (2011); Sofi et al. (2019); Shahadat et al. (2017); Visakh y Thomas (2010); Selvalakshmi et al. (2017); Goel et al. (2023); Kumar et al. (2022); Vibha y Negi (2020); Kanatt y Makwana (2020); Das A. et al. (2022); Thulasisingh et al. (2022); Kaur et al. (2020); Tambawala et al. (2022); Umesh et al. (2022); Priyadarsini et al. (2021); Manimohan et al. (2020a); Aquinas et al. (2022); Agrawal et al. (2022); Gasti et al. (2021). |
|  | PLA | Sangeetha et al. (2018); Sharmila et al. (2013). |
|  | PHA | Mathuriya y Yakhmi (2017). |
|  | QUITOSAN | Malhotra et al. (2015); Divakara et al. (2010); Narasagoudr et al. (2020); Yadav et al. (2020); Yadav et al. (2021); Manimohan et al. (2020b); Hiremani et al. (2022). |
|  | WPBA | Zafar et al. (2015). |
|  | MUCILAGOS | Rohini et al. (2020). |
|  | GELATINA | Sharma et al. (2021). |
|  | NANOCOMPUESTOS | Gupta et al. (2022); Thivya et al. (2021); Chaudhary et al. (2020); Kendre et al. (2022). |
| INDONESIA Total (2) | QUITOSAN | El-Gamal et al. (2018). |
|  | NANOCOMPUESTOS | Hasan et al. (2019). |
| IRAN Total (9) | ALGINATO | Dekamin et al. (2018). |
|  | CELULOSA | Erfani et al. (2022); Abdulkhani et al. (2020). |
|  | BIOPOLIMEROS | Alizadeh-Sani et al. (2020); Karimi et al. (2020); Ghasempour et al. (2022) |
|  | NANOCOMPUESTOS | Janani et al. (2020); Zahiri Oghani et al. (2021); Sherafatkhah et al. (2021). |
| IRAQ | QUITOSAN | Ahmed K. K. et al. (2022). |
| IRLANDA Total (2) | BIOPOLIMEROS | Khodaei et al. (2021); Garavand et al. (2022). |
| ITALIA Total (5) | CELULOSA | Rovera et al. (2018). |
|  | PLA | Trombino et al. (2012); Scaffaro et al. (2016). |
|  | QUITOSAN | Rossi et al. (2013). |
|  | NANO PARTICULAS | De Marco (2022). |
|  | BIOPOLIMEROS | Marassi et al. (2021). |
| KOREA Total (2) | PP-PM | Basavaraja et al. (2010). |
|  | CELULOSA | Rukmanikrishnan et al. (2021). |
| MALASIA Total (5) | PLA | Bakri et al. (2018). |
|  | PHA | Hema et al. (2013). |
|  | QUITOSAN | Julkapli et al. (2011). |
|  | BIOPOLIMEROS | Asyraf et al. (2022); Mohd Basri et al. (2021). |
| MARRUECOS Total (2) | CELULOSA | El Achaby et al. (2018). |
|  | QUITOSAN | Orkhis y Ettaqi (2022). |
| MEXICO | QUITOSAN | Fonseca-García et al. (2021). |
| PAKISTAN Total (4) | PULLULAN | Tabasum et al. (2018). |
|  | PHA | Zia F. et al. (2015). |
|  | BIOPOLIMEROS | Faizan Muneer et al. (2021). |
|  | PVA | Asgher et al. (2020). |
| PERU | BIOPOLIMEROS | Torres et al. (2019). |
| POLONIA Total (9) | CELULOSA | Kowalczyk et al. (2015); Ciecholewska-Juśko et al. (2021). |
|  | BIOPOLIMEROS | Sikorska et al. (2017). |
|  | PROTEINA DE SUERO | Kawecka-Radomska et al. (2015). |
|  | PP-PM | Wiącek et al. (2017). |
|  | QUITOSAN | Jamróz et al. (2021). |
|  | ALGINATO | Kurczewska et al. (2021). |
|  | GELATINA | Tkaczewska et al. (2021). |
|  | NANOCOMPUESTOS | Bajer et al. (2020). |
| PORTUGAL Total (3) | PLA | Pinto et al. (2013). |
|  | ALGINATO | Lomartire et al. (2022). |
|  | CARRAGEENAN | Lomartire et al. (2022). |
| REP. DE KOREA Total (5) | PVA | Tak-H et al. (2019). |
|  | PULULAN | Lee et al. (2019); Priyadarshi et al. (2021). |
|  | PECTINA | Lee et al. (2019). |
|  | QUITOSAN | Kim J. et al. (2021). |
| RUSIA Total (3) | GELATINA | Vasil’ev (2007). |
|  | NANOPARTICULAS | Volkova et al. (2022). |
|  | BIOPOLIMEROS | Chursin y Lyubimtseva (2020). |
| SINGAPUR | PHA | Yeo et al. (2018). |
| SUIZA | CELULOSA | Hansen et al. (2012); Duval y Lawoko (2014). |
| SUR AFRICA | BIOPOLIMEROS | Ibrahim I. D. et al. (2022). |
| TAILANDIA Total (5) | GELATINA | Sukhlaaied y Riyajan (2018). |
|  | QUITOSAN | Sukhlaaied y Riyajan (2016); Soe et al. (2020). |
|  | BIOPOLIMEROS | Riyajan (2019); Singh et al. (2022). |
| TAIWAN Total (2) | PLA | Wu J. H. et al. (2016). |
|  | GELATINA | Wu L. T. et al. (2021). |
| TANZANIA | PHA | Mlalila et al. (2018). |
| UKRANIA | NANOCOMPUESTOS | Barbash et al. (2022). |

  - Biopolímeros, Bio-basados y Naturales

La investigación sobre biopolímeros tiene una clasificación inicial según su origen. Es así que, los polímeros de base biológica provienen de materiales derivados de la biomasa como productos agrícolas, microorganismos, algas o crustáceos y polímeros parcialmente compuestos o sintetizados (Hottle et al. 2013). Para estos polímeros se identificaron 12 categorías según la materia prima, los reactivos y procesos químicos. Los cuales se subdividen en 30 insumos por el recurso del cual provienen; además, se han realizado 21 métodos de obtención o desarrollos tecnológicos. El polímero con mayor representación de base biológica es el Ácido Poliláctico con 10 insumos utilizados, seguido del Acetato de Polivinilo (PVA) con 9 insumos (Tabla 3).

Por otro lado, los polímeros naturales son macromoléculas que se pueden encontrar en la naturaleza como proteínas, polisacáridos, terpenos y lípidos (Sell et al. 2010). Según la revisión, los polímeros naturales se han dividido en ocho categorías, que a partir de los compuestos que extraen de los recursos naturales se subdivididen en 43 insumos, de los cuales se presentan 28 métodos de obtención o desarrollos tecnológicos. Es así que, la celulosa cuenta con 22 diferentes materias primas para su obtención y el chitosan con 18, por lo que son los elementos más representativos (Tabla 3).

Tabla 3. Clasificación de Biopolímeros

| TIPO DE POLIMERO | POLIMERO | RECURSODE ORIGEN | PRODUCTO / OBTENCIÓN | REFERENCIA |
| --- | --- | --- | --- | --- |
| NATURAL | ALGINATO | ALGAS | HIDROGELES | Serrano Aroca et al. (2018) |
|  |  |  | NEURTRALIZACION | Lomartire et al. (2022) |
|  | CARRAGEENAN | COCO BABASU | RETICULACIÓN | Tak et al. (2019) |
|  |  | MINERALES DE HALLOYSITA | ADSORBENTES | Kurczewska et al. (2021) |
|  |  | ALGAS | HIDROCOLOIDES | Lomartire et al. (2022) |
|  |  | HOJA DE OLIVO | EXTRACCIÓN POR MICROONDAS | da Rosa et al. (2020) |
|  | CELULOSA | FRUTAS | NANOTECNOLOGIA (PILOGENETICA) | Neera et al. (2015) |
|  |  |  | NANOFIBRAS | Sofi et al. (2019) |
|  |  | MADERA | NANOFIBRAS | Hansen et al. (2012) |
|  |  | PLANTAS | POLIMEROS REDORZADOS | Miao y Hamad (2013) |
|  |  | ALMIDON | BIOCOMPUESTOS | Gutiérrez y Alvarez (2017) |
|  |  | HONGOS | NANOCOMPUESTOS | Wang Y. et al. (2018) |
|  |  | RESIDUOS VEGETALES | DESFIBRILACION BACTERIANA | Meneguin et al. (2020) |
|  |  | CASCARA DE ARROZ | DIFRACCION RAYOS X | Elhussieny et al. (2020) |
|  |  | CANELA | EMULSION | Erfani et al. (2022) |
|  |  | BACTERIAS DE CELULOSA | RETICULACIÓN | Ciecholewska-Juśko et al. (2021) |
|  |  | S NEEI (PLANTA) | EXTRACCION Y FRACCIONAMIENTO | Villarreal et al. (2021) |
|  |  | XILANO | DIFRACCION RAYOS X | Abdulkhani et al. (2020) |
|  |  | SILICE | DIFRACCION RAYOS X | Rukmanikrishnan et al. (2021) |
|  |  | PLATA | DIFRACCION RAYOS X | Rukmanikrishnan et al. (2021) |
|  |  | FIBRAS DE COCO | ESPECTROSCOPIA INFRARROJA | Gupta et al. (2022) |
|  |  | CASCARA DE CACAHUATE | ESPECTROSCOPIA INFRARROJA | Gupta et al. (2022) |
|  |  | ARRURRUZ | NANOEMULSION | de Oliveira et al. (2021) |
|  |  | BAMBU | DIFRACCION RAYOS X | Hasan et al. (2019) |
|  |  | LECHUGA DE AGUA | MICROSCOPIA LEECTRONICA DE BARRIDO | Umesh et al. (2022) |
|  |  | TALLO DE CHALOTA | EXTRACCION ASISTIDA POR MICROONDAS | Thivya et al. (2021) |
|  |  | SEMILLAS DE TAMARINDO | EXTRACCION ASISTIDA POR MICROONDAS | Thivya et al. (2021) |
|  |  | AGAR | ESPECTROSCOPIA INFRARROJA | Kalyani y Khandelwal (2021) |
|  |  | CAÑAMO | ESPECTROSCOPIA INFRARROJA | Barbash et al. (2022) |
|  | MUCILAGOS | OCIMUM BACILICUM | DIFRACCION RAYOS X | Rohini et al. (2020) |
| NATURAL | QUITOSAN | ALGAS | CATALIZADOR | Shahadat et al. (2017) |
|  |  |  | EMULSIONANANTE | Zia et al. (2017) |
|  |  |  | FIBRAS | Virtanen et al. (2017) |
|  |  | HONGOS | NANOCOMPUESTOS | Shahadat et al. (2017) |
|  |  | MADERA (EUCALIPTO) | NANOCOMPUESTOS | Wiącek et al. (2017) |
|  |  | CANGREGO,KRILL, CAMARON | POLIMEROS REDORZADOS | Divakara et al. (2010) |
|  |  | ALMIDON DE MAIZ | DIFRACCION RAYOS X | Fonseca-García et al. (2021) |
|  |  | RESIDUOS DE CAMARON | RESONANCIA MAGNETICA NUCLEAR | Elhussieny et al. (2020) |
|  |  | HOJAS TE NEGRO | DIFRACCION RAYOS X | Ahmed K. et al. (2022) |
|  |  | FURCELLARAN | ESPECTROSCOPIA INFRARROJA | Jamróz et al. (2021) |
|  |  | ARROZ GLUTINOSO | DIFRACCION RAYOS X | Soe et al. (2020) |
|  |  | QUECENTINA | ESPECTROSCOPIA INFRARROJA | Yadav et al. (2020) |
|  |  | ACIDO GALICO | ESPECTROSCOPIA INFRARROJA | Yadav et al. (2021) |
|  |  | MELANINA | ENTRECRUCE MOLECULAR | Zhao et al. (2022) |
|  |  | SILICE | DIFRACCION RAYOS X | Dong et al. (2022) |
|  |  | HALLOYSITA | ELECTROHILADO | Zou-Y et al. (2020) |
|  |  | HOJA DE ORTIGA | ESPECTROSCOPIA INFRARROJA | Zahiri Oghani et al. (2021) |
|  |  | ACIDO CITRICO | DIFRACCION RAYOS X | Favatela et al. (2022) |
|  |  | SCHIFF | DIFRACCION RAYOS X | Manimohan et al. (2020a) |
|  |  | PLUMA DE POLLO | ESPECTROSCOPIA INFRARROJA | Orkhis y Ettaqi (2022) |
|  | GELATINA | CAUCHO SECO | SOLUCION DE LATEX | Sukhlaaied y Riyajan (2016) |
|  |  | GELATINA | FRUTOS BAEL | Sharma et al. (2021) |
|  |  | PIEL DE CARPA | HIDROLIZADO | Tkaczewska et al. (2021) |
|  |  | GELLAN GUM | ESPECTROSCOPIA INFRARROJA | Wu L. et al. (2021) |
|  | PULLULAN | ALGAS | FIBRAS | Tabasum et al. (2018) |
|  |  |  | HIDROGLES | Tabasum et al. (2018) |
|  |  |  | NANOFIBRAS | Tabasum et al. (2018) |
|  |  | SOYA | FUNDICIÓN EN SOLUCIÓN | Lee et al. (2019) |
|  |  | PECTINA | FUNDICIÓN EN SOLUCIÓN | Priyadarshi et al. (2021) |
|  | PROTEINA DE SUERO | SUERO DE LECHE | GEL | Kawecka-Radomska et al. (2015). |
|  |  | GOMA PERSA | DIFRACCION RAYOS X | Ghasempour et al. (2022) |
| BIOBASE | POLICAPROLACTONA (PCL) | CAFÉ | EPOXIDOS (LIPIDOS) | Williamson y Hatzakis (2019) |
|  |  | ACEITE PLANTAS | ELECTROHILADO | Bhullar et al. (2015) |
|  | PLA (ACIDO POLILÁCTICO) | MAIZ | HIDROGELES | Duquette y Dumont (2019) |
|  |  |  | ELECTRICIDAS | Perez-Masia et al. (2013) |
|  |  |  | GOMAS | Zhang Q. et al. (2018) |
|  |  |  | FIBRAS | Scaffaro et al. (2016) |
|  |  |  | NANOCRISTALES | Scaffaro et al. (2017) |
|  |  |  | ESPUMA DE POLIMEROOS | Chauvet et al. (2017) |
|  |  | CAÑA AZUCAR | POLIMEROS REDORZADOS | Xian et al. (2018) |
|  |  | SEMILLA JACA | FIBRAS | Sharmila et al. (2013) |
|  |  | ACACIAS | POLIMEROS REDORZADOS | Bakri et al. (2018) |
|  |  | YUCA | POLIMEROS REDORZADOS | Sangeetha et al. (2018) |
|  |  | HONGOS | FIBRAS | Satam et al. (2018) |
|  |  | SOYA | FIBRAS | Janjarasskul y Krochta (2010) |
|  |  | MAIZ | REDISOLUCIÓN | Aznar et al. (2019) |
|  |  | OLIGOMEROS | EXTRACCION SORPCTIVA | Ubeda et al. (2021) |
|  |  | FIBRA DE LINO | MEZCLAS | Asyraf et al. (2022) |
|  | POLIFENOLES | TE NANOFIBRAS | ELECTRO HILADOS | Zhang D. et al. (2021) |
|  | POLIURETANO | QUITINA | DIFRACCION RAYOS X | Moustafa et al. (2022) |
|  |  | COLOFONIA | ESPECTROSCOPIA INFRARROJA | Moustafa et al. (2022) |
|  | PHA | COLAGENO | FIBRAS | Vasil’ev (2007) |
|  |  | BACTERIA CAPRIAVUDUS | NANOCOMPUESTOS | Hema et al. (2013) |
|  |  | BACTERIAS | POLIMEROS REDORZADOS | Yeo et al. (2018) |
|  |  | AGUAS RESIDUALES | ESPECTROSCOPIA INFRARROJA | Paul et al. (2021) |
|  |  | CASCARA DE YUCA | ELECTROHILADO | Vega-Castro et al. (2021) |
|  | PHA-PLG | MICROORGANISMOS (ALMIDON) | FIBRAS | Mlalila et al. (2018) |
|  |  | MICROORGANISMOS (HONGOS) | MORFOLOGIA 3D | Bandyopadhyay-Ghosh et al. (2018) |
|  | PBS-PBAT | ALMIDON | FIBRAS | Muthuraj et al. (2014) |
|  |  | FIBROINA DE SEDA | NANOFIBRAS ELECTRO HILADAS | He et al. (2020) |
|  | PHMC | MICROORGANISMOS | HIDROGEL | Hu et al. (2018) |
| BIOBASE | PPC | MICROORGANISMOS | ESPUMA DE POLIMEROOS | Henke et al. (2017) |
|  | PP-PM | MICROORGANISMOS | NANOCOMPUESTOS | Basavaraja et al. (2010) |
|  | PVA | MICROORGANISMOS | GEL | Silva et al. (2008) |
|  |  |  | PLASTIFICANTES | Silva et al. (2008) |
|  |  | PALMA ACEITERA | NANOFIBRAS | Solikhin et al. (2018) |
|  |  | NANO PARTICULAS DE SELENIO | DIFRACCION RAYOS X | Al-hakimi et al. (2022) |
|  |  | FRIJOL | SUNDILAC | Tak et al. (2019) |
|  |  | ALOE VERA | ESPECTROSCOPIA INFRARROJA | Kanatt y Makwana (2020) |
|  |  | CASCARA DE ARROZ | MICROSCOPIA ELECTRONICA DE BARRIDO | Asgher et al. (2020) |
|  |  | GLICEROL | ESPECTROSCOPIA INFRARROJA | Asgher et al. (2020) |
|  |  | ALGINATO DE SODIO | DIFUSION HIDROFILA | Singh et al. (2022) |
|  |  | GOMA GUARAN | DIFRACCION RAYOS X | Gasti et al. (2021) |
|  | WPBA | SEMILLAS VEGETALES | POLIMEROS REFORZADOS | Zafar et al. (2015) |

  - Aplicación de Biopolímeros

Los biopolímeros son compuestos de cadena larga que se componen de sub unidades de cadenas largas (Malhotra et al. 2015), debido a esta característica se han desarrollado múltiples investigaciones y descubierto diferentes usos para estos materiales. El método de obtención más común de los biopolímeros es a partir de la polimerización del compuesto básico, por ejemplo, almidones o nano-partículas de laboratorio, las cuales dan como resultado insumos útiles para diferentes aplicaciones.

De los artículos revisados, el biopolímero natural con mayor número de investigaciones hasta el 2022 es la celulosa con 22 diferentes desarrollos (Figura 2). Este polisacárido esta entre los biopolímeros más utilizados en la producción de películas biodegradables (Yu et al. 2019) por ser uno de los de mayor facilidad de extracción.

Fig. 2. Cantidad de recursos desarrollados como Biopolímeros

En cuanto a biopolímeros bio base, el ácido Poliláctico (PLA) presenta el mayor número de investigaciones con 10 diferentes procesos, esto se debe a sus aplicaciones versátiles industriales (John et al. 2009). La producción del ácido Poliláctico ha aumentado debido a su capacidad de compost y el uso de recursos renovables para su obtención. La producción biotecnológica de ácido láctico ofrece varias ventajas en comparación con la síntesis química, como el bajo costo de los sustratos, la baja temperatura de producción y el bajo consumo de energía (Madhavan Nampoothiri et al. 2010).

Los resultados muestran que, respecto al desarrollo de productos, el “empaque de alimentos” es la industria para la cual se han realizado más estudios, con 75 investigaciones diferentes (Figura 3). Es decir, del total de la muestra seleccionada, el 38% de los artículos relacionan el empaque de alimentos como un posible uso de los biopolímeros. Otro factor relevante es el aumento significativo año a año de hasta cinco veces más de investigaciones relacionadas a los materiales de empaque de alimentos de origen bio base. Este aumento en las investigaciones se presenta por el potencial que tienen los materiales en cuanto a sus características físicas y mecánicas para ser usados como polímeros en la industria de los empaques (Abdullah et al. 2022).

Fig. 3. Aplicación de Biopolímeros 2008-2022

El segundo ítem con mayor número de aplicaciones es la bio medicina, esto se debe principalmente a que los biopolímeros no presentan toxicidad y están autorizados para uso médico según la Administración de Alimentos y Medicamentos (FDA, por sus siglas en inglés Food and Drug Administration) de Estados Unidos (Philp et al. 2005).  Además, estos materiales han ofrecido respuestas para influir en la función metabólica de las células en una variedad de formas, dado que puede servir como un sustrato energético, por su carácter no cargado y su tamaño pequeño (Philp et al. 2005). También, presenta avances en la ingeniería de tejidos, como puente del tejido y la resistencia a la adhesión celular (Wang et al. 2007), e incluso se puede utilizar como hueso artificial, que el organismo es capaz de reabsorber (Pant et al. 2013).

En cuanto al desarrollo de envases para la industria farmacéutica el Ácido Poliláctico (PLA) es el material con mayor número de investigaciones destinadas a su uso como empaque farmacéutico (Tabla 4). La constancia sobre este material se debe a los efectos físico-mecánicos notables para aplicaciones industriales, al permitirle avanzar como material de empaque (Perez-Masia et al. 2015). Además, presenta aspectos de calidad como estabilidad, uniformidad del contenido y liberación del contenido, por otra parte, en cuanto a la resistencia mecánica pueden verse afectados durante las operaciones de procesamiento (Abreu et al. 2015).

Tabla 4. Biopolímeros utilizados para envases

| MATERIAL | METODO | PAÍS | AÑO | REFERENCIAS |
| --- | --- | --- | --- | --- |
| CELULOSA | ESPECTROSCOPIA INFRARROJA | INDIA | 2021 | Kalyani y Khandelwal |
| GELATINA | ESPECTROSCOPIA INFRARROJA | EGIPTO | 2021 | Ibrahim et al. |
| NANOCOMPUESTOS | MEZCLAS | INDIA | 2022 | Kendre et al. |
| NANOCOMPUESTOS | PRECIPITACION QUIMICA | ALEMANIA | 2019 | Ghanbari Adivi et al. |
| PHA | MEZCLAS | SUR AFRICA | 2022 | Ibrahim et al. |
| PLA | GRUPO FENOLICOS | ITALIA | 2012 | Trombino, et al. |
| PLA | ESPECTROSCOPIA INFRARROJA | IRAN | 2020 | Karimi et al. |
| PLA | ELECTROHILADO | HUNGRIA | 2022 | Yi et al. |
| PLA | HIDROLISIS | CHINA | 2018 | Xian et al. |
| PULLULAN | MICROSCOPIA ELECTRÓNICA DE BARRIDO | PAKISTAN | 2018 | Tabasum et al. |
| PVA | ESPECTROSCOPIA INFRARROJA | TAILANDIA | 2019 | Riyajan |
| QUITOSAN | DIFRACCION RAYOS X | TAILANDIA | 2020 | Soe et al. |

Otro biopolímero que presenta excelente respuesta en el empaque de productos farmacéuticos es el Poli (Alcohol Vinílico) de Pullulan, es un biopolímero bio-compatible y no tóxico que se puede obtener como solvente y utilizar como material de embalaje de medicamentos (Tabasum et al. 2018).

- Conclusiones

Existe una tendencia muy alta en realizar investigaciones sobre biopolímeros en los últimos años. Por ejemplo, India es el país con el mayor número de investigaciones de la muestra analizada, donde existe una profundización académica sobre el tema. Además, se logró identificar dos tipos de bipolimero, de acuerdo a su origen: (1) Los de base biológica, que presentan 21 metodos de desarrollo tecnológico y de obtención. Precisamente, el Ácido Poliláctico (PLA) y el Acetato de Polivinilo (PVA) son los de mayor representación. Y (2) los de base natural, con 28 métodos, al ser la celulosa y el chitosan los más utilizados.

Así mismo, de la información analizada entre los años 2008 hasta 2022, las investigaciones sobre biopolímeros tienen un comportamiento ascendente, en algunos casos en una proporción de 5 a 1 con el año anterior. Los países con mayor número de publicaciones son India, China y Brasil respectivamente, con una participación de 60 de los 196 artículos revisados.

En la actualidad los biopolímeros son una posibilidad real para remplazar los plásticos convencionales derivados del petróleo. Esta investigación demuestra que se han utilizado 43 materiales de origen Bio base para el desarrollo de biopolímeros, con 28 formas de obtención diferentes e investigado 41 usos de sus potenciales aplicaciones.

De acuerdo a relación sobre las posibles aplicaciones de los biopolímeros, se encontró como tendencia, que las investigaciones realizadas se dirigen a su posible uso como empaques de alimentos y la biomedicina, dadas sus características físicas y mecánicas en estos campos, además de que no son tóxicos y presentan posibilidades de bioasimilación con el cuerpo humano.

Así mismo, el Ácido Poliláctico (PLA) con 4 aplicaciones como empaque farmacéutico es el biopolímero más desarrollado hasta ahora, por su maleabilidad y síntesis con otros materiales al bio-asimilarlo, lo que permite reforzar sus características para maximizar y mejorar sus usos. Su fabricación a partir de sub productos agrícolas genera una disponibilidad suficiente para su desarrollo industrial, no produce contaminación atmosférica en su fabricación y minimiza la generación de residuos por su característica compostable.

En las diferentes investigaciones revisadas, los biopolímeros se mezclan con otros insumos para evitar que se interfiera con el propósito del medicamento, por tanto, la clave para determinar cuál es el material idóneo como envase de medicamentos está en las mezclas exitosas de los bio polímeros con otros materiales que permita la estabilidad del producto y pueda ser avalado para este uso.

Referencias

Abdulkhani, A., Najd Mazhar, A., Hedjazi, S., & Hamzeh, Y. (2020). Preparation of xylan bio-composite films reinforced with oxidized carboxymethyl cellulose and nanocellulose. Polymer Bulletin, 77(12), 6227-6239. https://doi.org/10.1007/s00289-019-03075-5

Abdullah, J. A. A., Jiménez-Rosado, M., Benítez, J. J., Guerrero, A., & Romero, A. (2022). Biopolymer-Based Films Reinforced with FexOy-Nanoparticles. Polymers, 14(21), 4487. https://doi.org/10.3390/polym14214487

Abreu, A. S., Oliveira, M., de Sá, A., Rodrigues, R. M., Cerqueira, M. A., Vicente, A. A., & Machado, A. V. (2015). Antimicrobial nanostructured starch based films for packaging. Carbohydrate Polymers, 129, 127-134. https://doi.org/10.1016/j.carbpol.2015.04.021

Abutalib, M. M., & Rajeh, A. (2021). Enhanced structural, electrical, mechanical properties and antibacterial activity of Cs/PEO doped mixed nanoparticles (Ag/TiO2) for food packaging applications. Polymer Testing, 93, 107013. https://doi.org/10.1016/j.polymertesting.2020.107013

Agrawal, R., Kumar, A., Singh, S., & Sharma, K. (2022). Recent advances and future perspectives of lignin biopolymers. Journal of Polymer Research, 29(6), 222. https://doi.org/10.1007/s10965-022-03068-5

Ahmed, K. K., Hussen, S. A., & Aziz, S. B. (2022). Transferring the wide band gap chitosan: POZ-based polymer blends to small optical energy band gap polymer composites through the inclusion of green synthesized Zn2+-PPL metal complex. Arabian Journal of Chemistry, 15(7), 103913. https://doi.org/10.1016/j.arabjc.2022.103913

Ahmed, M. K., Moydeen, A. M., Ismail, A. M., El-Naggar, M. E., Menazea, A. A., & El-Newehy, M. H. (2021). Wound dressing properties of functionalized environmentally biopolymer loaded with selenium nanoparticles. Journal of Molecular Structure, 1225, 129138. https://doi.org/10.1016/j.molstruc.2020.129138

Akhlaghi, S. P., Berry, R. C., & Tam, K. C. (2013). Surface modification of cellulose nanocrystal with chitosan oligosaccharide for drug delivery applications. Cellulose, 20(4), 1747-1764. https://doi.org/10.1007/s10570-013-9954-y

Al-hakimi, A. N., Asnag, G. M., Alminderej, F., Alhagri, I. A., Al-Hazmy, S. M., & Abdallah, E. M. (2022). Enhanced structural, optical, electrical properties and antibacterial activity of selenium nanoparticles loaded PVA/CMC blend for electrochemical batteries and food packaging applications. Polymer Testing, 116, 107794. https://doi.org/10.1016/j.polymertesting.2022.107794

Alizadeh-Sani, M., Mohammadian, E., & McClements, D. J. (2020). Eco-friendly active packaging consisting of nanostructured biopolymer matrix reinforced with TiO2 and essential oil: Application for preservation of refrigerated meat. Food Chemistry, 322, 126782. https://doi.org/10.1016/j.foodchem.2020.126782

AL-Oqla, F. M., Alaaeddin, M. H., Hoque, M. E., & Thakur, V. K. (2022). Biopolymers and Biomimetic Materials in Medical and Electronic-Related Applications for Environment–Health–Development Nexus: Systematic Review. Journal of Bionic Engineering, 19(6), 1562-1577. https://doi.org/10.1007/s42235-022-00240-x

Alves Lopes, I., Coelho Paixão, L., Souza da Silva, L. J., Almeida Rocha, A., D. Barros Filho, A. K., & Amorim Santana, A. (2020). Elaboration and characterization of biopolymer films with alginate and babassu coconut mesocarp. Carbohydrate Polymers, 234, 115747. https://doi.org/10.1016/j.carbpol.2019.115747

Ansorena, M. R., Marcovich, N. E., & Pereda, M. (2018). Food Biopackaging Based on Chitosan. En L. M. T. Martínez, O. V. Kharissova, & B. I. Kharisov (Eds.), Handbook of Ecomaterials (pp. 1-27). Springer International Publishing. https://doi.org/10.1007/978-3-319-48281-1_68-1

Aquinas, N., Bhat M, R., & Selvaraj, S. (2022). A review presenting production, characterization, and applications of biopolymer curdlan in food and pharmaceutical sectors. Polymer Bulletin, 79(9), 6905-6927. https://doi.org/10.1007/s00289-021-03860-1

Asgher, M., Nasir, I., Khalid, N., & Qamar, S. A. (2020). Development of biocomposites based on bacterial cellulose reinforced delignified rice husk-PVA plasticized with glycerol. Journal of Polymer Research, 27(11), 347. https://doi.org/10.1007/s10965-020-02314-y

Asyraf, M. R. M., Ishak, M. R., Norrrahim, M. N. F., Amir, A. L., Nurazzi, N. M., Ilyas, R. A., Asrofi, M., Rafidah, M., & Razman, M. R. (2022). Potential of Flax Fiber Reinforced Biopolymer Composites for Cross-Arm Application in Transmission Tower: A Review. Fibers and Polymers, 23(4), 853-877. https://doi.org/10.1007/s12221-022-4383-x

Auras, R., Harte, B., & Selke, S. (2004). An Overview of Polylactides as Packaging Materials. Macromolecular Bioscience, 4(9), 835-864. https://doi.org/10.1002/mabi.200400043

Aznar, M., Ubeda, S., Dreolin, N., & Nerín, C. (2019). Determination of non-volatile components of a biodegradable food packaging material based on polyester and polylactic acid (PLA) and its migration to food simulants. Journal of Chromatography A, 1583, 1-8. https://doi.org/10.1016/j.chroma.2018.10.055

Bajer, D., Janczak, K., & Bajer, K. (2020). Novel Starch/Chitosan/Aloe Vera Composites as Promising Biopackaging Materials. Journal of Polymers and the Environment, 28(3), 1021-1039. https://doi.org/10.1007/s10924-020-01661-7

Bakri, M. K. B., Jayamani, E., Hamdan, S., Rahman, Md. R., & Kakar, A. (2018). Potential of Borneo Acacia wood in fully biodegradable bio-composites’ commercial production and application. Polymer Bulletin, 75(11), 5333-5354. https://doi.org/10.1007/s00289-018-2299-9

Bandyopadhyay-Ghosh, S., Ghosh, S. B., Rodríguez, A., & Sain, M. M. (2018). Biosynthesis, Microstructural Characterisations and Investigation of In-Vitro Mutagenic and Eco-Toxicological Response of a Novel Microbial Exopolysaccharide Based Biopolymer. Journal of Polymers and the Environment, 26(1), 365-374. https://doi.org/10.1007/s10924-016-0925-x

Barbash, V. A., Yashchenko, O. V., Yakymenko, O. S., Zakharko, R. M., & Myshak, V. D. (2022). Preparation of hemp nanocellulose and its use to improve the properties of paper for food packaging. Cellulose, 29(15), 8305-8317. https://doi.org/10.1007/s10570-022-04773-6

Bardin, L. (1996). El análisis de contenido (C. Suárez, Trad.; 2.a ed.). Akal Ediciones.

Basavaraja, C., Veeranagouda, Y., Lee, K., Vishnuvardhan, T. K., Pierson, R., & Huh, D. S. (2010). Synthesis and characterization of conducting polypyrrole-polymannuronate nanocomposites. Journal of Polymer Research, 17(2), 233-239. https://doi.org/10.1007/s10965-009-9309-4

Bhullar, S. K., Kaya, B., & Jun, M. B.-G. (2015). Development of Bioactive Packaging Structure Using Melt Electrospinning. Journal of Polymers and the Environment, 23(3), 416-423. https://doi.org/10.1007/s10924-015-0713-z

Biswas, M. C., Jony, B., Nandy, P. K., Chowdhury, R. A., Halder, S., Kumar, D., Ramakrishna, S., Hassan, M., Ahsan, M. A., Hoque, M. E., & Imam, M. A. (2022). Recent Advancement of Biopolymers and Their Potential Biomedical Applications. Journal of Polymers and the Environment, 30(1), 51-74. https://doi.org/10.1007/s10924-021-02199-y

Borja, J. M., & Eva, S. J. (2006). Recopilación bibliográfica de materiales de envase primario, secundario y terciario, para las formas farmacéuticas liquidas, sólidas y semisólidas [Tesis de Pregrado]. Universidad de El Salvador.

Chaudhary, P., Fatima, F., & Kumar, A. (2020). Relevance of Nanomaterials in Food Packaging and its Advanced Future Prospects. Journal of Inorganic and Organometallic Polymers and Materials, 30(12), 5180-5192. https://doi.org/10.1007/s10904-020-01674-8

Chauvet, M., Sauceau, M., & Fages, J. (2017). Extrusion assisted by supercritical CO 2: A review on its application to biopolymers. The Journal of Supercritical Fluids, 120, 408-420. https://doi.org/10.1016/j.supflu.2016.05.043

Chow, K., Tong, H. H. Y., Lum, S., & Chow, A. H. L. (2008). Engineering of Pharmaceutical Materials: An Industrial Perspective. Journal of Pharmaceutical Sciences, 97(8), 2855-2877. https://doi.org/10.1002/jps.21212

Chursin, V. I., & Lyubimtseva, E. S. (2020). Effect of Polysaccharide Constituents on the Properties of Biopolymer Composites and Films Based on Them. Fibre Chemistry, 51(5), 362-367. https://doi.org/10.1007/s10692-020-10112-x

Correa, S., Dreaden, E. C., Gu, L., & Hammond, P. T. (2016). Engineering nanolayered particles for modular drug delivery. Journal of Controlled Release, 240, 364-386. https://doi.org/10.1016/j.jconrel.2016.01.040

da Rosa, G. S., Vanga, S. K., Gariepy, Y., & Raghavan, V. (2020). Development of Biodegradable Films with Improved Antioxidant Properties Based on the Addition of Carrageenan Containing Olive Leaf Extract for Food Packaging Applications. Journal of Polymers and the Environment, 28(1), 123-130. https://doi.org/10.1007/s10924-019-01589-7

Darensbourg, D. J. (2011). Book Review of Poly(Lactic Acid): Synthesis, Structures, Properties, Processing, and Applications. Journal of the American Chemical Society, 133(18), 7237-7237. https://doi.org/10.1021/ja203078c

Das, A., Ringu, T., Ghosh, S., & Pramanik, N. (2022). A comprehensive review on recent advances in preparation, physicochemical characterization, and bioengineering applications of biopolymers. Polymer Bulletin. https://doi.org/10.1007/s00289-022-04443-4

Davis, G., & Song, J. H. (2006). Biodegradable packaging based on raw materials from crops and their impact on waste management. Industrial Crops and Products, 23(2), 147-161. https://doi.org/10.1016/j.indcrop.2005.05.004

De Marco, I. (2022). Zein Microparticles and Nanoparticles as Drug Delivery Systems. Polymers, 14(11), 2172. https://doi.org/10.3390/polym14112172

de Mesquita, J. P., Donnici, C. L., & Pereira, F. V. (2010). Biobased Nanocomposites from Layer-by-Layer Assembly of Cellulose Nanowhiskers with Chitosan. Biomacromolecules, 11(2), 473-480. https://doi.org/10.1021/bm9011985

de Oliveira Filho, J. G., Albiero, B. R., Cipriano, L., de Oliveira Nobre Bezerra, C. C., Oldoni, F. C. A., Egea, M. B., de Azeredo, H. M. C., & Ferreira, M. D. (2021). Arrowroot starch-based films incorporated with a carnauba wax nanoemulsion, cellulose nanocrystals, and essential oils: A new functional material for food packaging applications. Cellulose, 28(10), 6499-6511. https://doi.org/10.1007/s10570-021-03945-0

Dekamin, M. G., Karimi, Z., Latifidoost, Z., Ilkhanizadeh, S., Daemi, H., Naimi-Jamal, M. R., & Barikani, M. (2018). Alginic acid: A mild and renewable bifunctional heterogeneous biopolymeric organocatalyst for efficient and facile synthesis of polyhydroquinolines. International Journal of Biological Macromolecules, 108, 1273-1280. https://doi.org/10.1016/j.ijbiomac.2017.11.050

Divakara, S., Siddaraju, G. N., & Somashekar, R. (2010). Comparative study of natural and man-made polymers using whole powder pattern fitting technique. Fibers and Polymers, 11(6), 861-868. https://doi.org/10.1007/s12221-010-0861-7

Dong, W., Su, J., Chen, Y., Xu, D., Cheng, L., Mao, L., Gao, Y., & Yuan, F. (2022). Characterization and antioxidant properties of chitosan film incorporated with modified silica nanoparticles as an active food packaging. Food Chemistry, 373, 131414. https://doi.org/10.1016/j.foodchem.2021.131414

Duquette, D., & Dumont, M.-J. (2019). Comparative studies of chemical crosslinking reactions and applications of bio-based hydrogels. Polymer Bulletin, 76(5), 2683-2710. https://doi.org/10.1007/s00289-018-2516-6

Duval, A., & Lawoko, M. (2014). A review on lignin-based polymeric, micro- and nano-structured materials. Reactive and Functional Polymers, 85, 78-96. https://doi.org/10.1016/j.reactfunctpolym.2014.09.017

El Achaby, M., El Miri, N., Hannache, H., Gmouh, S., Trabadelo, V., Aboulkas, A., & Ben Youcef, H. (2018). Cellulose nanocrystals from Miscanthus fibers: Insights into rheological, physico-chemical properties and polymer reinforcing ability. Cellulose, 25(11), 6603-6619. https://doi.org/10.1007/s10570-018-2047-1

El-Gamal, S., El Sayed, A. M., & Abdel-Hady, E. E. (2018). Effect of Cobalt Oxide Nanoparticles on the Nano-scale Free Volume and Optical Properties of Biodegradable CMC/PVA Films. Journal of Polymers and the Environment, 26(6), 2536-2545. https://doi.org/10.1007/s10924-017-1151-x

Elhussieny, A., Faisal, M., D’Angelo, G., Aboulkhair, N. T., Everitt, N. M., & Fahim, I. S. (2020). Valorisation of shrimp and rice straw waste into food packaging applications. Ain Shams Engineering Journal, 11(4), 1219-1226. https://doi.org/10.1016/j.asej.2020.01.008

Erfani, A., Khalil Pirouzifard, M., Almasi, H., Gheybi, N., & Pirsa, S. (2022). Application of cellulose plate modified with encapsulated Cinnamomum zelanicum essential oil in active packaging of walnut kernel. Food Chemistry, 381, 132246. https://doi.org/10.1016/j.foodchem.2022.132246

Faizan Muneer, Nadeem, H., Arif, A., & Zaheer, W. (2021). Bioplastics from Biopolymers: An Eco-Friendly and Sustainable Solution of Plastic Pollution. Polymer Science, Series C, 63(1), 47-63. https://doi.org/10.1134/S1811238221010057

Farris, S., Schaich, K. M., Liu, L., Piergiovanni, L., & Yam, K. L. (2009). Development of polyion-complex hydrogels as an alternative approach for the production of bio-based polymers for food packaging applications: A review. Trends in Food Science & Technology, 20(8), 316-332. https://doi.org/10.1016/j.tifs.2009.04.003

Fasciotti, M. (2017). Perspectives for the use of biotechnology in green chemistry applied to biopolymers, fuels and organic synthesis: From concepts to a critical point of view. Sustainable Chemistry and Pharmacy, 6, 82-89. https://doi.org/10.1016/j.scp.2017.09.002

Favatela, M. F., Otarola, J., Ayala-Peña, V. B., Dolcini, G., Perez, S., Torres Nicolini, A., Alvarez, V. A., & Lassalle, V. L. (2022). Development and Characterization of Antimicrobial Textiles from Chitosan-Based Compounds: Possible Biomaterials Against SARS-CoV-2 Viruses. Journal of Inorganic and Organometallic Polymers and Materials, 32(4), 1473-1486. https://doi.org/10.1007/s10904-021-02192-x

Fernández, F. (2002). El análisis de contenido como ayuda metodológica para la investigación. Revista de Ciencias Sociales, II(96), 35-53.

Fonseca-García, A., Jiménez-Regalado, E. J., & Aguirre-Loredo, R. Y. (2021). Preparation of a novel biodegradable packaging film based on corn starch-chitosan and poloxamers. Carbohydrate Polymers, 251, 117009. https://doi.org/10.1016/j.carbpol.2020.117009

Friedrich, D. (2022). Success factors of Wood-Plastic Composites (WPC) as sustainable packaging material: A cross-sector expert study. Sustainable Production and Consumption, 30, 506-517. https://doi.org/10.1016/j.spc.2021.12.030

Garavand, F., Khodaei, D., Mahmud, N., Islam, J., Khan, I., Jafarzadeh, S., Tahergorabi, R., & Cacciotti, I. (2022). Recent progress in using zein nanoparticles-loaded nanocomposites for food packaging applications. Critical Reviews in Food Science and Nutrition, 1-21. https://doi.org/10.1080/10408398.2022.2133080

Gasti, T., Hiremani, V. D., Kesti, S. S., Vanjeri, V. N., Goudar, N., Masti, S. P., Thimmappa, S. C., & Chougale, R. B. (2021). Physicochemical and Antibacterial Evaluation of Poly (Vinyl Alcohol)/Guar Gum/Silver Nanocomposite Films for Food Packaging Applications. Journal of Polymers and the Environment, 29(10), 3347-3363. https://doi.org/10.1007/s10924-021-02123-4

Geyer, R., Jambeck, J. R., & Law, K. L. (2017). Production, use, and fate of all plastics ever made. Science Advances, 3(7), 1-5. https://doi.org/10.1126/sciadv.1700782

Ghanbari Adivi, F., Hashemi, P., & Dadkhah Tehrani, A. (2019). Agarose-coated Fe3O4@SiO2 magnetic nanoparticles modified with sodium dodecyl sulfate, a new promising sorbent for fast adsorption/desorption of cationic drugs. Polymer Bulletin, 76(3), 1239-1256. https://doi.org/10.1007/s00289-018-2418-7

Ghasempour, Z., Khodaeivandi, S., Ahangari, H., Hamishehkar, H., Amjadi, S., Moghaddas Kia, E., & Ehsani, A. (2022). Characterization and Optimization of Persian Gum/Whey Protein Bionanocomposite Films Containing Betanin Nanoliposomes for Food Packaging Utilization. Journal of Polymers and the Environment, 30(7), 2800-2811. https://doi.org/10.1007/s10924-021-02367-0

Goel, P., Arora, R., Haleem, R., & Shukla, S. K. (2023). Advances in Bio-degradable Polymer Composites-Based Packaging Material. Chemistry Africa, 6(1), 95-115. https://doi.org/10.1007/s42250-022-00404-6

Grondin, J. (2014). ¿Qué es la hermenéutica? (A. Martínez, Trad.). Herder Editorial. http://www.jstor.org/stable/10.2307/j.ctvt7x88s

Gupta, H., Kumar, H., Gehlaut, A. K., Singh, S. K., Gaur, A., Sachan, S., & Park, J.-W. (2022). Preparation and characterization of bio-composite films obtained from coconut coir and groundnut shell for food packaging. Journal of Material Cycles and Waste Management, 24(2), 569-581. https://doi.org/10.1007/s10163-021-01343-z

Gutiérrez, T. J., & Alvarez, V. A. (2017). Cellulosic materials as natural fillers in starch-containing matrix-based films: A review. Polymer Bulletin, 74(6), 2401-2430. https://doi.org/10.1007/s00289-016-1814-0

Hansen, N. M. L., Blomfeldt, T. O. J., Hedenqvist, M. S., & Plackett, D. V. (2012). Properties of plasticized composite films prepared from nanofibrillated cellulose and birch wood xylan. Cellulose, 19(6), 2015-2031. https://doi.org/10.1007/s10570-012-9764-7

Hasan, M., Lai, T. K., Gopakumar, D. A., Jawaid, M., Owolabi, F. A. T., Mistar, E. M., Alfatah, T., Noriman, N. Z., Haafiz, M. K. M., & Abdul Khalil, H. P. S. (2019). Micro Crystalline Bamboo Cellulose Based Seaweed Biodegradable Composite Films for Sustainable Packaging Material. Journal of Polymers and the Environment, 27(7), 1602-1612. https://doi.org/10.1007/s10924-019-01457-4

Hashim, S. B. H., Elrasheid Tahir, H., Liu, L., Zhang, J., Zhai, X., Ali Mahdi, A., Nureldin Awad, F., Hassan, M. M., Xiaobo, Z., & Jiyong, S. (2022). Intelligent colorimetric pH sensoring packaging films based on sugarcane wax/agar integrated with butterfly pea flower extract for optical tracking of shrimp freshness. Food Chemistry, 373, 131514. https://doi.org/10.1016/j.foodchem.2021.131514

Hema, R., Ng, P. N., & Amirul, A. A. (2013). Green nanobiocomposite: Reinforcement effect of montmorillonite clays on physical and biological advancement of various polyhydroxyalkanoates. Polymer Bulletin, 70(3), 755-771. https://doi.org/10.1007/s00289-012-0822-y

Henke, L., Zarrinbakhsh, N., Endres, H.-J., Misra, M., & Mohanty, A. K. (2017). Biodegradable and Bio-based Green Blends from Carbon Dioxide-Derived Bioplastic and Poly(Butylene Succinate). Journal of Polymers and the Environment, 25(2), 499-509. https://doi.org/10.1007/s10924-016-0828-x

Hernández Silva, M. L., & Guzmán Martínez, B. (2009). Biopolímeros empleados en la fabricación de envases para alimentos. Publicaciones e Investigación, 3(1), 103. https://doi.org/10.22490/25394088.572

Hernández, R., & Mendoza, C. P. (2018). Metodología de la investigación: Las rutas cuantitativa, cualitativa y mixta (1.a ed.). McGraw-Hill Interamericana Editores S. A. de C. V.

Hiremani, V. D., Gasti, T., Masti, S. P., Malabadi, R. B., & Chougale, R. B. (2022). Polysaccharide-based blend films as a promising material for food packaging applications: Physicochemical properties. Iranian Polymer Journal, 31(4), 503-518. https://doi.org/10.1007/s13726-021-01014-8

Hottle, T. A., Bilec, M. M., & Landis, A. E. (2013). Sustainability assessments of bio-based polymers. Polymer Degradation and Stability, 98(9), 1898-1907. https://doi.org/10.1016/j.polymdegradstab.2013.06.016

Hu, Y., Zhang, S., Han, D., Ding, Z., Zeng, S., & Xiao, X. (2018). Construction and evaluation of the hydroxypropyl methyl cellulose-sodium alginate composite hydrogel system for sustained drug release. Journal of Polymer Research, 25(7), 148. https://doi.org/10.1007/s10965-018-1546-y

Ibrahim, I. D., Hamam, Y., Sadiku, E. R., Ndambuki, J. M., Kupolati, W. K., Jamiru, T., Eze, A. A., & Snyman, J. (2022). Need for Sustainable Packaging: An Overview. Polymers, 14(20), 4430. https://doi.org/10.3390/polym14204430

Ibrahim, S., Elsayed, H., & Hasanin, M. (2021). Biodegradable, Antimicrobial and Antioxidant Biofilm for Active Packaging Based on Extracted Gelatin and Lignocelluloses Biowastes. Journal of Polymers and the Environment, 29(2), 472-482. https://doi.org/10.1007/s10924-020-01893-7

Imre, B., & Pukánszky, B. (2013). Compatibilization in bio-based and biodegradable polymer blends. European Polymer Journal, 49(6), 1215-1233. https://doi.org/10.1016/j.eurpolymj.2013.01.019

Jamróz, E., Janik, M., Juszczak, L., Kruk, T., Kulawik, P., Szuwarzyński, M., Kawecka, A., & Khachatryan, K. (2021). Composite biopolymer films based on a polyelectrolyte complex of furcellaran and chitosan. Carbohydrate Polymers, 274, 118627. https://doi.org/10.1016/j.carbpol.2021.118627

Janani, N., Zare, E. N., Salimi, F., & Makvandi, P. (2020). Antibacterial tragacanth gum-based nanocomposite films carrying ascorbic acid antioxidant for bioactive food packaging. Carbohydrate Polymers, 247, 116678. https://doi.org/10.1016/j.carbpol.2020.116678

Janjarasskul, T., & Krochta, J. M. (2010). Edible Packaging Materials. Annual Review of Food Science and Technology, 1(1), 415-448. https://doi.org/10.1146/annurev.food.080708.100836

Jayaramudu, J., Reddy, G. S. M., Varaprasad, K., Sadiku, E. R., Sinha Ray, S., & Varada Rajulu, A. (2013). Preparation and properties of biodegradable films from Sterculia urens short fiber/cellulose green composites. Carbohydrate Polymers, 93(2), 622-627. https://doi.org/10.1016/j.carbpol.2013.01.032

Jiang, J., Chen, X., Zhang, G.-L., Hao, H., Hou, H.-M., & Bi, J. (2022). Preparation of chitosan-cellulose-benzyl isothiocyanate nanocomposite film for food packaging applications. Carbohydrate Polymers, 285, 119234. https://doi.org/10.1016/j.carbpol.2022.119234

Johansson, C., Bras, J., Mondragon, I., Nechita, P., Plackett, D., Šimon, P., Svetec, D. G., Virtanen, S., Baschetti, M. G., Breen, C., Clegg, F., & Aucejo, S. (2012). Renewable fibers and bio-based materials for packaging applications—A review of recent developments. Bioresources, 7(2), 2506-2552. https://doi.org/10.15376/biores.7.2.2506-2552

John, R. P., G.S., A., Nampoothiri, K. M., & Pandey, A. (2009). Direct lactic acid fermentation: Focus on simultaneous saccharification and lactic acid production. Biotechnology Advances, 27(2), 145-152. https://doi.org/10.1016/j.biotechadv.2008.10.004

Julkapli, N. M., Ahmad, Z., & Akil, H. M. (2011). Effects of different pH medium on swelling properties of 1,2,4,5-benzenetetracarboxylic-chitosan-filled chitosan bio-composites. Polymer Bulletin, 67(2), 291-320. https://doi.org/10.1007/s00289-010-0424-5

Kale, G., Auras, R., Singh, S. P., & Narayan, R. (2007). Biodegradability of polylactide bottles in real and simulated composting conditions. Polymer Testing, 26(8), 1049-1061. https://doi.org/10.1016/j.polymertesting.2007.07.006

Kale, G., Kijchavengkul, T., Auras, R., Rubino, M., Selke, S. E., & Singh, S. P. (2007). Compostability of Bioplastic Packaging Materials: An Overview. Macromolecular Bioscience, 7(3), 255-277. https://doi.org/10.1002/mabi.200600168

Kalyani, P., & Khandelwal, M. (2021). Modulation of morphology, water uptake/retention, and rheological properties by in-situ modification of bacterial cellulose with the addition of biopolymers. Cellulose, 28(17), 11025-11036. https://doi.org/10.1007/s10570-021-04256-0

Kanatt, S. R., & Makwana, S. H. (2020). Development of active, water-resistant carboxymethyl cellulose-poly vinyl alcohol-Aloe vera packaging film. Carbohydrate Polymers, 227, 115303. https://doi.org/10.1016/j.carbpol.2019.115303

Karimi, M., Yazdi, F. T., Mortazavi, S. A., Shahabi-Ghahfarrokhi, I., & Chamani, J. (2020). Development of active antimicrobial poly (l-glutamic) acid-poly (l-lysine) packaging material to protect probiotic bacterium. Polymer Testing, 83, 106338. https://doi.org/10.1016/j.polymertesting.2020.106338

Kaufman, L., & Rousseeuw, P. J. (2005). Finding groups in data: An introduction to cluster analysis. Wiley.

Kaur, A., Singh, D., & Sud, D. (2020). A review on grafted, crosslinked and composites of biopolymer Xanthan gum for phasing out synthetic dyes and toxic metal ions from aqueous solutions. Journal of Polymer Research, 27(10), 297. https://doi.org/10.1007/s10965-020-02271-6

Kawecka-Radomska, M., Tomczyńska-Mleko, M., Wesołowska-Trojanowska, M., Kowalczyk, K., Chrząstek, M., & Mleko, S. (2015). Hard Biodegradable Biopolymer Obtained from Whey Protein Concentrate and Montmorillonite. Journal of Polymers and the Environment, 23(4), 534-540. https://doi.org/10.1007/s10924-015-0722-y

Kendre, P. N., Gite, M., Jain, S. P., & Pote, A. (2022). Nanocomposite polymeric materials: State of the art in the development of biomedical drug delivery systems and devices. Polymer Bulletin, 79(11), 9237-9265. https://doi.org/10.1007/s00289-021-03985-3

Khodaei, D., Álvarez, C., & Mullen, A. M. (2021). Biodegradable Packaging Materials from Animal Processing Co-Products and Wastes: An Overview. Polymers, 13(15), 2561. https://doi.org/10.3390/polym13152561

Kim, J., Kim, T. H., Lee, J. H., Park, Y. Ah., Kang, Y. J., & Ji, H. G. (2021). Porous nanocomposite of layered double hydroxide nanosheet and chitosan biopolymer for cosmetic carrier application. Applied Clay Science, 205, 106067. https://doi.org/10.1016/j.clay.2021.106067

Kostag, M., Gericke, M., Heinze, T., & El Seoud, O. A. (2019). Twenty-five years of cellulose chemistry: Innovations in the dissolution of the biopolymer and its transformation into esters and ethers. Cellulose, 26(1), 139-184. https://doi.org/10.1007/s10570-018-2198-0

Kowalczyk, D., Kordowska-Wiater, M., Sołowiej, B., & Baraniak, B. (2015). Physicochemical and Antimicrobial Properties of Biopolymer-Candelilla Wax Emulsion Films Containing Potassium Sorbate – A Comparative Study. Food and Bioprocess Technology, 8(3), 567-579. https://doi.org/10.1007/s11947-014-1423-6

Kumar, A. P., Depan, D., Singh Tomer, N., & Singh, R. P. (2009). Nanoscale particles for polymer degradation and stabilization—Trends and future perspectives. Progress in Polymer Science, 34(6), 479-515. https://doi.org/10.1016/j.progpolymsci.2009.01.002

Kumar, S., Kalita, S., Das, A., Kumar, P., Singh, S., Katiyar, V., & Mukherjee, A. (2022). Aloe vera: A contemporary overview on scope and prospects in food preservation and packaging. Progress in Organic Coatings, 166, 106799. https://doi.org/10.1016/j.porgcoat.2022.106799

Kurczewska, J., Ratajczak, M., & Gajecka, M. (2021). Alginate and pectin films covering halloysite with encapsulated salicylic acid as food packaging components. Applied Clay Science, 214, 106270. https://doi.org/10.1016/j.clay.2021.106270

Lagaron, J. M., & Lopez-Rubio, A. (2011). Nanotechnology for bioplastics: Opportunities, challenges and strategies. Trends in Food Science & Technology, 22(11), 611-617. https://doi.org/10.1016/j.tifs.2011.01.007

Lagarón, J.-M., & Busolo, M.-A. (2011). Multifunctional nanoclays for food contact applications. En Multifunctional and Nanoreinforced Polymers for Food Packaging (pp. 31-42). Elsevier. https://doi.org/10.1533/9780857092786.1.31

Lee, J. H., Jeong, D., & Kanmani, P. (2019). Study on physical and mechanical properties of the biopolymer/silver based active nanocomposite films with antimicrobial activity. Carbohydrate Polymers, 224, 115159. https://doi.org/10.1016/j.carbpol.2019.115159

Liarou, E., Varlas, S., Skoulas, D., Tsimblouli, C., Sereti, E., Dimas, K., & Iatrou, H. (2018). Smart polymersomes and hydrogels from polypeptide-based polymer systems through α-amino acid N-carboxyanhydride ring-opening polymerization. From chemistry to biomedical applications. Progress in Polymer Science, 83, 28-78. https://doi.org/10.1016/j.progpolymsci.2018.05.001

Lomartire, S., Marques, J. C., & Gonçalves, A. M. M. (2022). An Overview of the Alternative Use of Seaweeds to Produce Safe and Sustainable Bio-Packaging. In Applied Sciences (Switzerland) (Vol. 12, Issue 6). MDPI. https://doi.org/10.3390/app12063123

Lopes, M. S., Jardini, A. L., & Filho, R. M. (2012). Poly (Lactic Acid) Production for Tissue Engineering Applications. Procedia Engineering, 42, 1402-1413. https://doi.org/10.1016/j.proeng.2012.07.534

López-Noguero, F. (2002). El análisis de contenido como método de investigación. Revista de Educación, XXI(4), 167-179.

Luckachan, G. E., & Pillai, C. K. S. (2011). Biodegradable Polymers- A Review on Recent Trends and Emerging Perspectives. Journal of Polymers and the Environment, 19(3), 637-676. https://doi.org/10.1007/s10924-011-0317-1

Madhavan Nampoothiri, K., Nair, N. R., & John, R. P. (2010). An overview of the recent developments in polylactide (PLA) research. Bioresource Technology, 101(22), 8493-8501. https://doi.org/10.1016/j.biortech.2010.05.092

Malhotra, B., Keshwani, A., & Kharkwal, H. (2015). Natural polymer based cling films for food packaging. 7(4), 10-18.

Mallakpour, S., & Asadi, P. (2012). Synthesis and structural characterization of novel bionanocomposite poly(ester-imide)s containing TiO2 nanoparticles, S-valine, and l-tyrosine amino acids moieties. Polymer Bulletin, 68(1), 53-67. https://doi.org/10.1007/s00289-011-0519-7

Manimohan, M., Pugalmani, S., & Sithique, M. A. (2020a). Biologically Active Water Soluble Novel Biopolymer/Hydrazide Based O-Carboxymethyl Chitosan Schiff Bases: Synthesis and Characterisation. Journal of Inorganic and Organometallic Polymers and Materials, 30(9), 3658-3676. https://doi.org/10.1007/s10904-020-01487-9

Manimohan, M., Pugalmani, S., & Sithique, M. A. (2020b). Synthesis, Spectral Characterisation and Biological Activities of Novel Biomaterial/N, N, O Donor Tridentate Co (II), Ni (II) and Zn (II) Complexes of Hydrazide Based Biopolymer Schiff Base Ligand. Journal of Inorganic and Organometallic Polymers and Materials, 30(11), 4481-4495. https://doi.org/10.1007/s10904-020-01578-7

Marassi, V., De Marchis, F., Roda, B., Bellucci, M., Capecchi, A., Reschiglian, P., Pompa, A., & Zattoni, A. (2021). Perspectives on protein biopolymers: Miniaturized flow field-flow fractionation-assisted characterization of a single-cysteine mutated phaseolin expressed in transplastomic tobacco plants. Journal of Chromatography A, 1637, 461806. https://doi.org/10.1016/j.chroma.2020.461806

Martin, O., & Avérous, L. (2001). Poly(lactic acid): Plasticization and properties of biodegradable multiphase systems. Polymer, 42(14), 6209-6219. https://doi.org/10.1016/S0032-3861(01)00086-6

Martínez, L. M. T., Kharissova, O. V., & Kharisov, B. I. (Eds.). (2019). Handbook of Ecomaterials. Springer International Publishing. https://doi.org/10.1007/978-3-319-68255-6

Mathuriya, A. S., & Yakhmi, J. V. (2017). Polyhydroxyalkanoates: Biodegradable Plastics and Their Applications. En L. M. T. Martínez, O. V. Kharissova, & B. I. Kharisov (Eds.), Handbook of Ecomaterials (pp. 1-29). Springer International Publishing. https://doi.org/10.1007/978-3-319-48281-1_84-1

Meeks, D., Hottle, T., Bilec, M. M., & Landis, A. E. (2015). Compostable biopolymer use in the real world: Stakeholder interviews to better understand the motivations and realities of use and disposal in the US. Resources, Conservation and Recycling, 105, 134-142. https://doi.org/10.1016/j.resconrec.2015.10.022

Mekonnen, T., Mussone, P., Khalil, H., & Bressler, D. (2013). Progress in bio-based plastics and plasticizing modifications. Journal of Materials Chemistry A, 1(43), 13379. https://doi.org/10.1039/c3ta12555f

Mellinas, C., Valdés, A., Ramos, M., Burgos, N., Garrigós, M. del C., & Jiménez, A. (2015). Active edible films: Current state and future trends. Journal of Applied Polymer Science, 133(2), n/a-n/a. https://doi.org/10.1002/app.42631

Meneguin, A. B., da Silva Barud, H., Sábio, R. M., de Sousa, P. Z., Manieri, K. F., de Freitas, L. A. P., Pacheco, G., Alonso, J. D., & Chorilli, M. (2020). Spray-dried bacterial cellulose nanofibers: A new generation of pharmaceutical excipient intended for intestinal drug delivery. Carbohydrate Polymers, 249, 116838. https://doi.org/10.1016/j.carbpol.2020.116838

Miao, C., & Hamad, W. Y. (2013). Cellulose reinforced polymer composites and nanocomposites: A critical review. Cellulose, 20(5), 2221-2262. https://doi.org/10.1007/s10570-013-0007-3

Mishra, D., Khare, P., Singh, D. K., Yadav, V., Luqman, S., Kumar, P. V. A., & Shanker, K. (2021). Synthesis of Ocimum extract encapsulated cellulose nanofiber/chitosan composite for improved antioxidant and antibacterial activities. Carbohydrate Polymer Technologies and Applications, 2, 100152. https://doi.org/10.1016/j.carpta.2021.100152

Mishra, R. K., Sabu, A., & Tiwari, S. K. (2018). Materials chemistry and the futurist eco-friendly applications of nanocellulose: Status and prospect. Journal of Saudi Chemical Society, 22(8), 949-978. https://doi.org/10.1016/j.jscs.2018.02.005

Mlalila, N., Hilonga, A., Swai, H., Devlieghere, F., & Ragaert, P. (2018). Antimicrobial packaging based on starch, poly(3-hydroxybutyrate) and poly(lactic-co-glycolide) materials and application challenges. Trends in Food Science & Technology, 74, 1-11. https://doi.org/10.1016/j.tifs.2018.01.015

Mohd Basri, M. S., Abdul Karim Shah, N. N., Sulaiman, A., Mohamed Amin Tawakkal, I. S., Mohd Nor, M. Z., Ariffin, S. H., Abdul Ghani, N. H., & Mohd Salleh, F. S. (2021). Progress in the Valorization of Fruit and Vegetable Wastes: Active Packaging, Biocomposites, By-Products, and Innovative Technologies Used for Bioactive Compound Extraction. Polymers, 13(20), 3503. https://doi.org/10.3390/polym13203503

Mooibroek, H., Oosterhuis, N., Giuseppin, M., Toonen, M., Franssen, H., Scott, E., Sanders, J., & Steinbüchel, A. (2007). Assessment of technological options and economical feasibility for cyanophycin biopolymer and high-value amino acid production. Applied Microbiology and Biotechnology, 77(2), 257-267. https://doi.org/10.1007/s00253-007-1178-3

Moustafa, H., Darwish, N. A., & Youssef, A. M. (2022). Rational formulations of sustainable polyurethane/chitin/rosin composites reinforced with ZnO-doped-SiO2 nanoparticles for green packaging applications. Food Chemistry, 371, 131193. https://doi.org/10.1016/j.foodchem.2021.131193

Muthuraj, R., Misra, M., & Mohanty, A. K. (2014). Biodegradable Poly(butylene succinate) and Poly(butylene adipate-co-terephthalate) Blends: Reactive Extrusion and Performance Evaluation. Journal of Polymers and the Environment, 22(3), 336-349. https://doi.org/10.1007/s10924-013-0636-5

Narasagoudr, S. S., Hegde, V. G., Vanjeri, V. N., Chougale, R. B., & Masti, S. P. (2020). Ethyl vanillin incorporated chitosan/poly(vinyl alcohol) active films for food packaging applications. Carbohydrate Polymers, 236, 116049. https://doi.org/10.1016/j.carbpol.2020.116049

Neera, Ramana, K. V., & Batra, H. V. (2015). Occurrence of Cellulose-Producing Gluconacetobacter spp. In Fruit Samples and Kombucha Tea, and Production of the Biopolymer. Applied Biochemistry and Biotechnology, 176(4), 1162-1173. https://doi.org/10.1007/s12010-015-1637-8

Núñez-Gómez, D., Rodrigues, C., Lapolli, F. R., & Lobo-Recio, M. A. (2021). Physicochemical Characterization of White Shrimp (Litopenaeus vannamei) Waste as a Low-Cost Chitinous Biomaterial. Journal of Polymers and the Environment, 29(2), 576-587. https://doi.org/10.1007/s10924-020-01887-5

Orantes, J. M. B., & Hernández, S. J. E. (2006). Recopilación bibliográfica de materiales de envase primario, secundario y terciario, para las formas farmacéuticas liquidas, sólidas y semisólidas. Universidad de el salvador, 1-331.

Orkhis, S., & Ettaqi, S. (2022). Effects of Alkali Treatment on Mechanical Properties of Chicken Feather Fiber/Chitosan Composites for Packaging Applications. Waste and Biomass Valorization, 13(4), 2309-2320. https://doi.org/10.1007/s12649-021-01630-8

Ortega-Santiago, Y., Julio-Rivas, S. A., Gómez, J.-M. P.-, & Lozano-Rivera, D. (2023). El Ecodiseño: Un llamado a la conciencia en el uso de polímeros biodegradables y no biodegradables. Gestión y Ambiente, 26(1), 1-12. https://doi.org/10.15446/ga.v26n1.110077

Oyarce, E., Cantero-López, P., Yañez, O., Roa, K., Boulett, A., Pizarro, G. D. C., Zhang, Y., Xu, C., Willför, S., & Sánchez, J. (2022). Nanocellulose bio-based composites for the removal of methylene blue from water: An experimental and theoretical exploration. Journal of Molecular Liquids, 357, 119089. https://doi.org/10.1016/j.molliq.2022.119089

Pant, H. R., Risal, P., Park, C. H., Tijing, L. D., Jeong, Y. J., & Kim, C. S. (2013). Core–shell structured electrospun biomimetic composite nanofibers of calcium lactate/nylon-6 for tissue engineering. Chemical Engineering Journal, 221, 90-98. https://doi.org/10.1016/j.cej.2013.01.072

Parente, A. G., de Oliveira, H. P., Cabrera, M. P., & de Morais Neri, D. F. (2023). Bio-based polymer films with potential for packaging applications: A systematic review of the main types tested on food. Polymer Bulletin, 80(5), 4689-4717. https://doi.org/10.1007/s00289-022-04332-w

Paul, E., Bessière, Y., Dumas, C., & Girbal-Neuhauser, E. (2021). Biopolymers Production from Wastes and Wastewaters by Mixed Microbial Cultures: Strategies for Microbial Selection. Waste and Biomass Valorization, 12(8), 4213-4237. https://doi.org/10.1007/s12649-020-01252-6

Perez-Masia, R., Lopez-Rubio, A., Fabra, M. J., & Lagaron, J. M. (2013). Biodegradable polyester-based heat management materials of interest in refrigeration and smart packaging coatings. Journal of Applied Polymer Science, 130(5), 3251-3262. https://doi.org/10.1002/app.39555

Perez-Masia, R., Ruben Lopez-Nicolas, Maria Jesús Periago, Gaspar Ros, Jose, Maria Lagaron, & Amparo Lopez-Rubio. (2015). Encapsulation of folic acid in food hydrocolloids through nanospray drying and electrospraying  for nutraceutical applications. 1-36.

Philp, A., Macdonald, A. L., & Watt, P. W. (2005). Lactate – a signal coordinating cell and systemic function. Journal of Experimental Biology, 208(24), 4561-4575. https://doi.org/10.1242/jeb.01961

Pinto, A. M., Moreira, S., Gonçalves, I. C., Gama, F. M., Mendes, A. M., & Magalhães, F. D. (2013). Biocompatibility of poly(lactic acid) with incorporated graphene-based materials. Colloids and Surfaces B: Biointerfaces, 104, 229-238. https://doi.org/10.1016/j.colsurfb.2012.12.006

Priyadarshi, R., Kim, S.-M., & Rhim, J.-W. (2021). Pectin/pullulan blend films for food packaging: Effect of blending ratio. Food Chemistry, 347, 129022. https://doi.org/10.1016/j.foodchem.2021.129022

Priyadarsini, M., Biswal, T., & Dash, S. (2021). Biodegradable superabsorbent with potential biomedical application as drug delivery system of “pectin-g-P(AN-co-AM)/chicken eggshell” bio-composite. Polymer Bulletin, 78(11), 6337-6349. https://doi.org/10.1007/s00289-020-03424-9

Qiu, S., Zhou, Y., Waterhouse, G. I. N., Gong, R., Xie, J., Zhang, K., & Xu, J. (2021). Optimizing interfacial adhesion in PBAT/PLA nanocomposite for biodegradable packaging films. Food Chemistry, 334, 127487. https://doi.org/10.1016/j.foodchem.2020.127487

Quiles-Carrillo, L., Montanes, N., Lagaron, J. M., Balart, R., & Torres-Giner, S. (2019). In Situ Compatibilization of Biopolymer Ternary Blends by Reactive Extrusion with Low-Functionality Epoxy-Based Styrene–Acrylic Oligomer. Journal of Polymers and the Environment, 27(1), 84-96. https://doi.org/10.1007/s10924-018-1324-2

Rajan, K. P., Thomas, S. P., Gopanna, A., & Chavali, M. (2018). Polyhydroxybutyrate (PHB): A Standout Biopolymer for Environmental Sustainability. En L. M. T. Martínez, O. V. Kharissova, & B. I. Kharisov (Eds.), Handbook of Ecomaterials (pp. 1-23). Springer International Publishing. https://doi.org/10.1007/978-3-319-48281-1_92-1

Reddy, M. M., Vivekanandhan, S., Misra, M., Bhatia, S. K., & Mohanty, A. K. (2013). Biobased plastics and bionanocomposites: Current status and future opportunities. Progress in Polymer Science, 38(10-11), 1653-1689. https://doi.org/10.1016/j.progpolymsci.2013.05.006

Resano-Goizueta, I., Ashokan, B. K., Trezza, T. A., & Padua, G. W. (2018). Effect of Nano-Fillers on Tensile Properties of Biopolymer Films. Journal of Polymers and the Environment, 26(9), 3817-3823. https://doi.org/10.1007/s10924-018-1260-1

Rhim, J.-W., & Ng, P. K. W. (2007). Natural Biopolymer-Based Nanocomposite Films for Packaging Applications. Critical Reviews in Food Science and Nutrition, 47(4), 411-433. https://doi.org/10.1080/10408390600846366

Rincón, E., Espinosa, E., García-Domínguez, M. T., Balu, A. M., Vilaplana, F., Serrano, L., & Jiménez-Quero, A. (2021). Bioactive pectic polysaccharides from bay tree pruning waste: Sequential subcritical water extraction and application in active food packaging. Carbohydrate Polymers, 272, 118477. https://doi.org/10.1016/j.carbpol.2021.118477

Riyajan, S.-A. (2019). Environmentally Friendly Novel Maleated Poly(vinyl alcohol) Grafted 1, 4-Butanediol Modified with Biopolymer for Encapsulation of Capsaicin. Journal of Polymers and the Environment, 27(11), 2637-2649. https://doi.org/10.1007/s10924-019-01542-8

Rodrigues, C., de Mello, J. M. M., Dalcanton, F., Macuvele, D. L. P., Padoin, N., Fiori, M. A., Soares, C., & Riella, H. G. (2020). Mechanical, Thermal and Antimicrobial Properties of Chitosan-Based-Nanocomposite with Potential Applications for Food Packaging. Journal of Polymers and the Environment, 28(4), 1216-1236. https://doi.org/10.1007/s10924-020-01678-y

Rodríguez-Sánchez, I. J., Fuenmayor, C. A., Clavijo-Grimaldo, D., & Zuluaga-Domínguez, C. M. (2021). Electrospinning of ultra-thin membranes with incorporation of antimicrobial agents for applications in active packaging: A review. International Journal of Polymeric Materials and Polymeric Biomaterials, 70(15), 1053-1076. https://doi.org/10.1080/00914037.2020.1785450

Rohini, B., Padma Ishwarya, S., Rajasekharan, R., & VijayaKumar, A. K. (2020). Ocimum basilicum seed mucilage reinforced with montmorillonite for preparation of bionanocomposite film for food packaging applications. Polymer Testing, 87, 106465. https://doi.org/10.1016/j.polymertesting.2020.106465

Rossi, S., Faccendini, A., Bonferoni, M. C., Ferrari, F., Sandri, G., Del Fante, C., Perotti, C., & Caramella, C. M. (2013). “Sponge-like” dressings based on biopolymers for the delivery of platelet lysate to skin chronic wounds. International Journal of Pharmaceutics, 440(2), 207-215. https://doi.org/10.1016/j.ijpharm.2012.07.056

Rovera, C., Cozzolino, C. A., Ghaani, M., Morrone, D., Olsson, R. T., & Farris, S. (2018). Mechanical behavior of biopolymer composite coatings on plastic films by depth-sensing indentation – A nanoscale study. Journal of Colloid and Interface Science, 512, 638-646. https://doi.org/10.1016/j.jcis.2017.10.108

Rukmanikrishnan, B., Ramalingam, S., Kim, S. S., & Lee, J. (2021). Rheological and anti-microbial study of silica and silver nanoparticles-reinforced k-carrageenan/hydroxyethyl cellulose composites for food packaging applications. Cellulose, 28(9), 5577-5590. https://doi.org/10.1007/s10570-021-03873-z

Sangeetha, V. H., Deka, H., Varghese, T. O., & Nayak, S. K. (2018). State of the art and future prospectives of poly(lactic acid) based blends and composites. Polymer Composites, 39(1), 81-101. https://doi.org/10.1002/pc.23906

Satam, C. C., Irvin, C. W., Lang, A. W., Jallorina, J. C. R., Shofner, M. L., Reynolds, J. R., & Meredith, J. C. (2018). Spray-Coated Multilayer Cellulose Nanocrystal—Chitin Nanofiber Films for Barrier Applications. ACS Sustainable Chemistry & Engineering, 6(8), 10637-10644. https://doi.org/10.1021/acssuschemeng.8b01536

Scaffaro, R., Botta, L., Lopresti, F., Maio, A., & Sutera, F. (2017). Polysaccharide nanocrystals as fillers for PLA based nanocomposites. Cellulose, 24(2), 447-478. https://doi.org/10.1007/s10570-016-1143-3

Scaffaro, R., Botta, L., Maio, A., Mistretta, M., & La Mantia, F. (2016). Effect of Graphene Nanoplatelets on the Physical and Antimicrobial Properties of Biopolymer-Based Nanocomposites. Materials, 9(5), 351. https://doi.org/10.3390/ma9050351

Scholten, E., Moschakis, T., & Biliaderis, C. G. (2014). Biopolymer composites for engineering food structures to control product functionality. Food Structure, 1(1), 39-54. https://doi.org/10.1016/j.foostr.2013.11.001

Sell, S. A., Wolfe, P. S., Garg, K., McCool, J. M., Rodriguez, I. A., & Bowlin, G. L. (2010). The Use of Natural Polymers in Tissue Engineering: A Focus on Electrospun Extracellular Matrix Analogues. Polymers, 2(4), 522-553. https://doi.org/10.3390/polym2040522

Selvalakshmi, S., Mathavan, T., Selvasekarapandian, S., & Premalatha, M. (2017). Study on NH4I composition effect in agar–agar-based biopolymer electrolyte. Ionics, 23(10), 2791-2797. https://doi.org/10.1007/s11581-016-1952-2

Serrano-Aroca, Á., Iskandar, L., & Deb, S. (2018). Green synthetic routes to alginate-graphene oxide composite hydrogels with enhanced physical properties for bioengineering applications. European Polymer Journal, 103, 198-206. https://doi.org/10.1016/j.eurpolymj.2018.04.015

Shahadat, M., Khan, M. Z., Rupani, P. F., Embrandiri, A., Sultana, S., Ahammad, S. Z., Wazed Ali, S., & Sreekrishnan, T. R. (2017). A critical review on the prospect of polyaniline-grafted biodegradable nanocomposite. Advances in Colloid and Interface Science, 249, 2-16. https://doi.org/10.1016/j.cis.2017.08.006

Sharma, B., Sandilya, A., Patel, U., Shukla, A., & Sadhu, S. D. (2021). A bio-inspired exploration of eco-friendly bael gum and guar gum-based bioadhesive as tackifiers for packaging applications. International Journal of Adhesion and Adhesives, 110, 102946. https://doi.org/10.1016/j.ijadhadh.2021.102946

Sharmila, G., Muthukumaran, C., Nayan, G., & Nidhi, B. (2013). Extracellular Biopolymer Production by Aureobasidium pullulans MTCC 2195 Using Jackfruit Seed Powder. Journal of Polymers and the Environment, 21(2), 487-494. https://doi.org/10.1007/s10924-012-0459-9

Shen, J., Fatehi, P., & Ni, Y. (2014). Biopolymers for surface engineering of paper-based products. Cellulose, 21(5), 3145-3160. https://doi.org/10.1007/s10570-014-0380-6

Sherafatkhah Azari, S., Alizadeh, A., Roufegarinejad, L., Asefi, N., & Hamishehkar, H. (2021). Preparation and characterization of gelatin/β-glucan nanocomposite film incorporated with ZnO nanoparticles as an active food packaging system. Journal of Polymers and the Environment, 29(4), 1143-1152. https://doi.org/10.1007/s10924-020-01950-1

Shtilman, M. I. (2010). Polymers for medicobiological use. Polymer Science Series A, 52(9), 884-899. https://doi.org/10.1134/S0965545X10090038

Sikorska, W., Musioł, M., Zawidlak-Węgrzyńska, B., & Rydz, J. (2017). Compostable Polymeric Ecomaterials: Environment-Friendly Waste Management Alternative to Landfills. En L. M. T. Martínez, O. V. Kharissova, & B. I. Kharisov (Eds.), Handbook of Ecomaterials (pp. 1-31). Springer International Publishing. https://doi.org/10.1007/978-3-319-48281-1_36-1

Silva, G. G. D., Sobral, P. J. A., Carvalho, R. A., Bergo, P. V. A., Mendieta-Taboada, O., & Habitante, A. M. Q. B. (2008). Biodegradable Films Based on Blends of Gelatin and Poly (Vinyl Alcohol): Effect of PVA Type or Concentration on Some Physical Properties of Films. Journal of Polymers and the Environment, 16(4), 276-285. https://doi.org/10.1007/s10924-008-0112-9

Singh, S., Chunglok, W., Nwabor, O. F., Ushir, Y. V., Singh, S., & Panpipat, W. (2022). Hydrophilic Biopolymer Matrix Antibacterial Peel-off Facial Mask Functionalized with Biogenic Nanostructured Material for Cosmeceutical Applications. Journal of Polymers and the Environment, 30(3), 938-953. https://doi.org/10.1007/s10924-021-02249-5

Siró, I., & Plackett, D. (2010). Microfibrillated cellulose and new nanocomposite materials: A review. Cellulose, 17(3), 459-494. https://doi.org/10.1007/s10570-010-9405-y

Soares, R. M. D., Siqueira, N. M., Prabhakaram, M. P., & Ramakrishna, S. (2018). Electrospinning and electrospray of bio-based and natural polymers for biomaterials development. Materials Science and Engineering: C, 92, 969-982. https://doi.org/10.1016/j.msec.2018.08.004

Soe, M. T., Pongjanyakul, T., Limpongsa, E., & Jaipakdee, N. (2020). Modified glutinous rice starch-chitosan composite films for buccal delivery of hydrophilic drug. Carbohydrate Polymers, 245, 116556. https://doi.org/10.1016/j.carbpol.2020.116556

Sofi, H. S., Ashraf, R., Khan, A. H., Beigh, M. A., Majeed, S., & Sheikh, F. A. (2019). Reconstructing nanofibers from natural polymers using surface functionalization approaches for applications in tissue engineering, drug delivery and biosensing devices. Materials Science and Engineering: C, 94, 1102-1124. https://doi.org/10.1016/j.msec.2018.10.069

Solikhin, A., Hadi, Y. S., Massijaya, M. Y., Nikmatin, S., Suzuki, S., Kojima, Y., & Kobori, H. (2018). Properties of Poly(Vinyl Alcohol)/Chitosan Nanocomposite Films Reinforced with Oil Palm Empty Fruit Bunch Amorphous Lignocellulose Nanofibers. Journal of Polymers and the Environment, 26(8), 3316-3333. https://doi.org/10.1007/s10924-018-1215-6

Sudesh, K., Abe, H., & Doi, Y. (2000). Synthesis, structure and properties of polyhydroxyalkanoates: Biological polyesters. Progress in Polymer Science, 25(10), 1503-1555. https://doi.org/10.1016/S0079-6700(00)00035-6

Sukhlaaied, W., & Riyajan, S.-A. (2016). Preparation and properties of a novel environmentally friendly film from maleated poly(vinyl alcohol) grafted with chitosan in solution form: The effect of different production factors. Polymer Bulletin, 73(3), 791-813. https://doi.org/10.1007/s00289-015-1520-3

Sukhlaaied, W., & Riyajan, S.-A. (2018). A Novel Environmentally Compatible Bio-Based Product from Gelatin and Natural Rubber: Physical Properties. Journal of Polymers and the Environment, 26(7), 2708-2719. https://doi.org/10.1007/s10924-017-1161-8

Tabasum, S., Noreen, A., Maqsood, M. F., Umar, H., Akram, N., Nazli, Z.-H., Chatha, S. A. S., & Zia, K. M. (2018). A review on versatile applications of blends and composites of pullulan with natural and synthetic polymers. International Journal of Biological Macromolecules, 120, 603-632. https://doi.org/10.1016/j.ijbiomac.2018.07.154

Tak, H.-Y., Yun, Y.-H., Lee, C.-M., & Yoon, S.-D. (2019). Sulindac imprinted mungbean starch/PVA biomaterial films as a transdermal drug delivery patch. Carbohydrate Polymers, 208, 261-268. https://doi.org/10.1016/j.carbpol.2018.12.076

Takács, T., Abdelghafour, M. M., Deák, Á., Szabó, D., Sebők, D., Dékány, I., Rovó, L., Kukovecz, Á., & Janovák, L. (2020). Surface wetting driven release of antifibrotic Mitomycin-C drug from modified biopolymer thin films. European Polymer Journal, 139, 109995. https://doi.org/10.1016/j.eurpolymj.2020.109995

Tambawala, H., Batra, S., Shirapure, Y., & More, A. P. (2022). Curcumin- A Bio-based Precursor for Smart and Active Food Packaging Systems: A Review. Journal of Polymers and the Environment, 30(6), 2177-2208. https://doi.org/10.1007/s10924-022-02372-x

Thakur, S., Chaudhary, J., Sharma, B., Verma, A., Tamulevicius, S., & Thakur, V. K. (2018). Sustainability of bioplastics: Opportunities and challenges. Current Opinion in Green and Sustainable Chemistry, 13, 68-75. https://doi.org/10.1016/j.cogsc.2018.04.013

Thivya, P., Bhosale, Y. K., Anandakumar, S., Hema, V., & Sinija, V. R. (2021). Exploring the Effective Utilization of Shallot Stalk Waste and Tamarind Seed for Packaging Film Preparation. Waste and Biomass Valorization, 12(10), 5779-5794. https://doi.org/10.1007/s12649-021-01402-4

Thulasisingh, A., Kumar, K., Yamunadevi, B., Poojitha, N., SuhailMadharHanif, S., & Kannaiyan, S. (2022). Biodegradable packaging materials. Polymer Bulletin, 79(7), 4467-4496. https://doi.org/10.1007/s00289-021-03767-x

Tkaczewska, J., Kulawik, P., Jamróz, E., Guzik, P., Zając, M., Szymkowiak, A., & Turek, K. (2021). One- and double-layered furcellaran/carp skin gelatin hydrolysate film system with antioxidant peptide as an innovative packaging for perishable foods products. Food Chemistry, 351, 129347. https://doi.org/10.1016/j.foodchem.2021.129347

Torres, F. G., Rodriguez, S., & Saavedra, A. C. (2019). Green Composite Materials from Biopolymers Reinforced with Agroforestry Waste. Journal of Polymers and the Environment, 27(12), 2651-2673. https://doi.org/10.1007/s10924-019-01561-5

Trombino, S., Cassano, R., Ferrarelli, T., Leta, S., Puoci, F., & Picci, N. (2012). Preparation, Characterization and Efficacy Evaluation of Synthetic Biocompatible Polymers Linking Natural Antioxidants. Molecules, 17(11), 12734-12745. https://doi.org/10.3390/molecules171112734

Ubeda, S., Aznar, M., Nerín, C., & Kabir, A. (2021). Fabric phase sorptive extraction for specific migration analysis of oligomers from biopolymers. Talanta, 233, 122603. https://doi.org/10.1016/j.talanta.2021.122603

Umesh, M., Santhosh, A. S., Shanmugam, S., Thazeem, B., Alharbi, S. A., Almoallim, H. S., Chi, N. T. L., & Pugazhendhi, A. (2022). Extraction, characterization, and fabrication of cellulose biopolymer sheets from Pistia stratiotes as a biodegradative coating material: An unique strategy for the conversion of invasive weeds into value-added products. Journal of Polymers and the Environment, 30(12), 5057-5068. https://doi.org/10.1007/s10924-022-02511-4

United Nations Environment Programme (UNEP). (2024). Global Waste Management Outlook 2024: Beyond an age of waste – Turning rubbish into a resource. https://www.unep.org/resources/global-waste-management-outlook-2024

Valbuena-Ussa, E. O. (2011). El Análisis de Contenido: De los manifiesto a lo oculto. En La investigación en ciencias sociales. Estrategias de investigación (1.a ed., pp. 211-222). Universidad Piloto de Colombia.

Vasilachis de Gialdino, I. (2006). La investigación cualitativa. En Estrategias de investigación cualitativa. Gedisa.

Vasil’ev, M. P. (2007). Basic scientific and practical results and prospects for development of collagen-based biomaterials. Fibre Chemistry, 39(2), 114-121. https://doi.org/10.1007/s10692-007-0025-8

Vega-Castro, O., León, E., Arias, M., Cesario, M. T., Ferreira, F., da Fonseca, M. M. R., Segura, A., Valencia, P., Simpson, R., Nuñez, H., & Contreras-Calderon, J. (2021). Characterization and Production of a Polyhydroxyalkanoate from Cassava Peel Waste: Manufacture of Biopolymer Microfibers by Electrospinning. Journal of Polymers and the Environment, 29(1), 187-200. https://doi.org/10.1007/s10924-020-01861-1

Vibha, K., & Negi, S. (2020). Enzymatic plasticising of lignin and styrene with adipic acid to synthesize a biopolymer with high antioxidant and thermostability. Polymer Degradation and Stability, 174, 109081. https://doi.org/10.1016/j.polymdegradstab.2020.109081

Vidović, E., Faraguna, F., & Jukić, A. (2017). Influence of inorganic fillers on PLA crystallinity and thermal properties. Journal of Thermal Analysis and Calorimetry, 127(1), 371–380. https://doi.org/10.1007/s10973-016-5750-x

Villarreal, M. R., Navarro, D. A., Ponce, N. M. A., Rojas, A. M., & Stortz, C. A. (2021). Perennial halophyte Salicornia neei Lag.: Cell wall composition and functional properties of its biopolymers. Food Chemistry, 350, 128659. https://doi.org/10.1016/j.foodchem.2020.128659

Virtanen, S., Chowreddy, R. R., Irmak, S., Honkapää, K., & Isom, L. (2017). Food Industry Co-streams: Potential Raw Materials for Biodegradable Mulch Film Applications. Journal of Polymers and the Environment, 25(4), 1110-1130. https://doi.org/10.1007/s10924-016-0888-y

Visakh, P. M., & Thomas, S. (2010). Preparation of Bionanomaterials and their Polymer Nanocomposites from Waste and Biomass. Waste and Biomass Valorization, 1(1), 121-134. https://doi.org/10.1007/s12649-010-9009-7

Volkova, T. V., Simonova, O. R., & Perlovich, G. L. (2022). Permeability of diverse drugs through a lipid barrier: Impact of pH and cyclodextrin. Journal of Molecular Liquids, 357, 119135. https://doi.org/10.1016/j.molliq.2022.119135

Wang, D.-Y., Li, H.-J., Chen, X., Nie, B.-L., & Wu, Y.-C. (2022). Fabricating of grape seed proanthocyanidins loaded Zein-NaCas composite nanoparticles to exert effective inhibition of Q235 steel corrosion in seawater. Journal of Molecular Liquids, 348, 118467. https://doi.org/10.1016/j.molliq.2022.118467

Wang, H., Li, Y., Zuo, Y., Li, J., Ma, S., & Cheng, L. (2007). Biocompatibility and osteogenesis of biomimetic nano-hydroxyapatite/polyamide composite scaffolds for bone tissue engineering. Biomaterials, 28(22), 3338-3348. https://doi.org/10.1016/j.biomaterials.2007.04.014

Wang, X., Qu, P., & Zhang, L. (2014). Thermal and structure properties of biobased cellulose nanowhiskers/poly (lactic acid) nanocomposites. Fibers and Polymers, 15(2), 302-306. https://doi.org/10.1007/s12221-014-0302-0

Wang, Y., Wang, X., Xie, Y., & Zhang, K. (2018). Functional nanomaterials through esterification of cellulose: A review of chemistry and application. Cellulose, 25(7), 3703-3731. https://doi.org/10.1007/s10570-018-1830-3

Wazzan, N. (2021). Adsorption of non-steroidal anti-inflammatory drugs (NSAIDs) on nanographene surface: Density functional theory study. Arabian Journal of Chemistry, 14(3), 103002. https://doi.org/10.1016/j.arabjc.2021.103002

Wiącek, A. E., Jurak, M., Gozdecka, A., & Worzakowska, M. (2017). Interfacial properties of PET and PET/starch polymers developed by air plasma processing. Colloids and Surfaces A: Physicochemical and Engineering Aspects, 532, 323-331. https://doi.org/10.1016/j.colsurfa.2017.04.074

Williamson, K., & Hatzakis, E. (2019). NMR analysis of roasted coffee lipids and development of a spent ground coffee application for the production of bioplastic precursors. Food Research International, 119, 683-692. https://doi.org/10.1016/j.foodres.2018.10.046

Wu, J.-H., Wu, C.-P., Kuo, M. C., & Tsai, Y. (2016). Characterization and Properties of Reactive Poly (Lactic Acid)/Ethylene–Vinyl Alcohol Copolymer Blends with Chain-Extender. Journal of Polymers and the Environment, 24(2), 129-138. https://doi.org/10.1007/s10924-016-0755-x

Wu, L.-T., Tsai, I.-L., Ho, Y.-C., Hang, Y.-H., Lin, C., Tsai, M.-L., & Mi, F.-L. (2021). Active and intelligent gellan gum-based packaging films for controlling anthocyanins release and monitoring food freshness. Carbohydrate Polymers, 254, 117410. https://doi.org/10.1016/j.carbpol.2020.117410

Xian, X., Wang, X., Zhu, Y., Guo, Y., & Tian, Y. (2018). Effects of MCC Content on the Structure and Performance of PLA/MCC Biocomposites. Journal of Polymers and the Environment, 26(8), 3484-3492. https://doi.org/10.1007/s10924-018-1226-3

Xie, L., Xu, H., Wang, Z.-P., Li, X.-J., Chen, J.-B., Zhang, Z.-J., Yin, H.-M., Zhong, G.-J., Lei, J., & Li, Z.-M. (2014). Toward faster degradation for natural fiber reinforced poly(lactic acid) biocomposites by enhancing the hydrolysis-induced surface erosion. Journal of Polymer Research, 21(3), 357. https://doi.org/10.1007/s10965-014-0357-z

Xing, H., Zhang, T., Pan, F., & Liu, J. (2021). Application of Electrochemically Synthesized Zinc Oxide Nanorods/Fava Bean Starch biocomposite in Food Active Packaging. International Journal of Electrochemical Science, 16(3), 210357. https://doi.org/https://doi.org/10.20964/2021.03.32

Yadav, S., Mehrotra, G. K., Bhartiya, P., Singh, A., & Dutta, P. K. (2020). Preparation, physicochemical and biological evaluation of quercetin based chitosan-gelatin film for food packaging. Carbohydrate Polymers, 227, 115348. https://doi.org/10.1016/j.carbpol.2019.115348

Yadav, S., Mehrotra, G. K., & Dutta, P. K. (2021). Chitosan based ZnO nanoparticles loaded gallic-acid films for active food packaging. Food Chemistry, 334, 127605. https://doi.org/10.1016/j.foodchem.2020.127605

Yeo, J. C. C., Muiruri, J. K., Thitsartarn, W., Li, Z., & He, C. (2018). Recent advances in the development of biodegradable PHB-based toughening materials: Approaches, advantages and applications. Materials Science and Engineering: C, 92, 1092-1116. https://doi.org/10.1016/j.msec.2017.11.006

Yi, L., Luo, S., Cui, L., Budai-Szűcs, M., Móczó, J., & Pukánszky, B. (2022). Processes taking place during the preparation and use of electrospun PLA fibers and their effect on controlled drug release. Journal of Thermal Analysis and Calorimetry, 147(23), 13191-13199. https://doi.org/10.1007/s10973-022-11554-7

York, A., Kirkland, S., & Mccormick, C. (2008). Advances in the synthesis of amphiphilic block copolymers via RAFT polymerization: Stimuli-responsive drug and gene delivery☆. Advanced Drug Delivery Reviews, 60(9), 1018-1036. https://doi.org/10.1016/j.addr.2008.02.006

Yu, J., Zhu, Y., Ma, H., Liu, L., Hu, Y., Xu, J., Wang, Z., & Fan, Y. (2019). Contribution of hemicellulose to cellulose nanofiber-based nanocomposite films with enhanced strength, flexibility and UV-blocking properties. Cellulose, 26(10), 6023-6034. https://doi.org/10.1007/s10570-019-02518-6

Zafar, F., Sharmin, E., Zafar, H., Shah, M. Y., Nishat, N., & Ahmad, S. (2015). Facile microwave-assisted preparation of waterborne polyesteramide/OMMT clay bio-nanocomposites for protective coatings. Industrial Crops and Products, 67, 484-491. https://doi.org/10.1016/j.indcrop.2015.01.057

Zahiri Oghani, F., Tahvildari, K., & Nozari, M. (2021). Novel Antibacterial Food Packaging Based on Chitosan Loaded ZnO Nano Particles Prepared by Green Synthesis from Nettle Leaf Extract. Journal of Inorganic and Organometallic Polymers and Materials, 31(1), 43-54. https://doi.org/10.1007/s10904-020-01621-7

Zhang, D., Chen, L., Cai, J., Dong, Q., Din, Z., Hu, Z.-Z., Wang, G.-Z., Ding, W.-P., He, J.-R., & Cheng, S.-Y. (2021). Starch/tea polyphenols nanofibrous films for food packaging application: From facile construction to enhance mechanical, antioxidant and hydrophobic properties. Food Chemistry, 360, 129922. https://doi.org/10.1016/j.foodchem.2021.129922

Zhang, Q., Li, D., Zhang, H., Su, G., & Li, G. (2018). Preparation and properties of poly(lactic acid)/sesbania gum/nano-TiO2 composites. Polymer Bulletin, 75(2), 623-635. https://doi.org/10.1007/s00289-017-2059-2

Zhang, Y., Chan, H. F., & Leong, K. W. (2013). Advanced materials and processing for drug delivery: The past and the future. Advanced Drug Delivery Reviews, 65(1), 104-120. https://doi.org/10.1016/j.addr.2012.10.003

Zhao, W., Liang, X., Wang, X., Wang, S., Wang, L., & Jiang, Y. (2022). Chitosan based film reinforced with EGCG loaded melanin-like nanocomposite (EGCG@MNPs) for active food packaging. Carbohydrate Polymers, 290, 119471. https://doi.org/10.1016/j.carbpol.2022.119471

Zia, F., Zia, K. M., Zuber, M., Kamal, S., & Aslam, N. (2015). Starch based polyurethanes: A critical review updating recent literature. Carbohydrate Polymers, 134, 784-798. https://doi.org/10.1016/j.carbpol.2015.08.034

Zia, K. M., Tabasum, S., Nasif, M., Sultan, N., Aslam, N., Noreen, A., & Zuber, M. (2017). A review on synthesis, properties and applications of natural polymer based carrageenan blends and composites. International Journal of Biological Macromolecules, 96, 282-301. https://doi.org/10.1016/j.ijbiomac.2016.11.095

Zou, Y., Zhang, C., Wang, P., Zhang, Y., & Zhang, H. (2020). Electrospun chitosan/polycaprolactone nanofibers containing chlorogenic acid-loaded halloysite nanotube for active food packaging. Carbohydrate Polymers, 247, 116711. https://doi.org/10.1016/j.carbpol.2020.116711

Administrador Ambiental y Magíster en Desarrollo Sustentable y Gestión Ambiental. Gerente Monser productos Farmacéuticos; correo electrónico: danielpinzon1992@gmail.com, ORCID: 0000-0003-3716-081X

Administrador Ambiental y Magíster en Derecho con énfasis en Recursos Naturales. Docente de la Universidad Distrital Francisco José de Caldas, Bogotá, Colombia, e integrante del Grupo de Investigación en Estudios Ambientales GEA-UD; correo electrónico: rodrigo.reyg@gmail.com; ORCID: 0000-0003-2650-9369